IMPERVIOUS SELECT MATERIAL:

Description

This work consists of furnishing, stockpiling, placing and maintaining impervious select material for stream plugs in locations as shown on the plans and cross-sections or as directed.

The quantity of Impervious Select Material to be installed will be affected by the actual conditions that occur during the construction of the project.  The quantity of Impervious Select Material may be increased, decreased, or eliminated entirely as directed.  Such variations in quantity will not be considered as alterations in the details of construction or a change in the character of the work.

Materials

Materials that will function as impervious barriers to water movement shall be a silty or clay soil material meeting the requirements of AASHTO M 145 for soil classification A-2, A-6 and A-7 provided such materials do not have a Liquid Limit (LL) greater than 50.  To maintain soil workability for placement and compaction, the following criteria shall apply for Plasticity Index (PI):

| Position of Borrow Material | Constraints on Plasticity Index (PI) |
| --- | --- |
| Below the water table | Must be greater than 7 and less than 25 |
| Above the water table | Must be greater than 7 and less than 35 |

Plasticity Index shall be determined in accordance with AASHTO T90 and the Liquid Limit shall be determined in accordance with AASHTO T89.  The Contractor is cautioned that soils tend to become less workable as the PI increases above 20.  Although a PI of 35 may be acceptable, the Contractor should be aware that additional efforts might be necessary to work the soil in order to achieve the minimum compaction standards.

Construction Methods

Impervious Select Material for stream plugs shall be constructed at locations as shown on the plans and cross-sections or as directed.  Impervious Select Material for stream plugs shall be used at the outlet end of uncompacted channel fills, and may be used at other locations to provide surface drainage relief from the uncompacted fills.

(A)	Clearing and Grubbing

Clear and Grub the stream plug cross-section on all sides to remove all vegetation and root mat material as directed to an elevation at least 1 ft. below the elevation of the existing channel cross-section.

(B)	Construction

Construct the stream plug using material that meets the requirements of the Materials section listed above.  Construct the stream plug to the dimensions detailed on the plans.

Measurement and Payment

Impervious Select Material will be measured and paid for as the actual number of cubic yards of material, measured in their original position and computed by the average end area method, which has been acceptably excavated in accordance with the plans and specifications.  Original cross-sections for the determination of the excavation quantities will be taken before any grading begins.  Final cross-sections will be taken after the excavation has been completed, except that the plan typical sections will be used for the final cross-sections where, in the opinion of the Engineer, the work has been constructed in reasonably close conformity to the plan typical section.  Original and final cross-sections will be taken by either ground or aerial survey methods, as determined by the Engineer.

Such price and payment will be full compensation for all work covered by this section, including but not limited to furnishing the source of the Impervious Select Material, providing and implementing a development, use and reclamation plan; building, maintaining and obliterating haul roads; clearing and grubbing the source; removal and disposition of overburden and other unsuitable material; excavation; hauling; restoration of the source and haul roads to an acceptable condition, seeding and mulching and maintaining the work.

Payment will be made under:

| Pay Item | #### Pay Unit |
| --- | --- |
| Impervious Select Material | Cubic Yard |