Standard Operating Procedure

2024 Ready Mixed Concrete Facility Annual Audit

# Objectives:

- The purpose of the Annual Facility Audit is to ensure that Ready Mixed Concrete facilities are operating and documenting correctly in operations that meet NCDOT standards and are capable of producing NCDOT approved concrete.

- Audits shall be performed a minimum of once per year, unannounced, and are recommended during NCDOT concrete production.

- Facilities that do not pass the Annual Facility Audit by the end of the calendar year without a significant reason could be removed from the NCDOT “Approved Facilities List”.

Materials Inspection and Acceptance:

The review of all documentation and collection of materials samples will confirm that the facility meets all NCDOT standards and is in compliance with all Materials and Tests Unit policies.

# Safety Concerns:

Personnel should always be aware of functioning equipment and machinery.  Review and follow all safety guidelines required by the facility.

# M&T Inspector’s Audit:

- View and verify an original (or a copy) 3rd party facility certificate to ensure it is active, signed, and on-site.

Record the 3rd party facility expiration date from the Certificate into the Audit Checklist.

- View and verify an original (or a copy) of the most current 3rd party inspection report. A copy of the completed report performed by the 3rd party shall be on-site. Record the inspection date into the Audit Checklist (the date shall not be more than 24 months ago).

- Verify whether the facility manager is sending all most current 3rd party inspection documentation to M&T. The email shall be submitted to readymixinspections@ncdot.gov.

- View and verify whether the facility is utilizing approved truck mixers. Note: inspection of the mixers shall be generated annually, and a copy of the report shall be kept on-site. Record the inspection expiration date in the audit checklist form. Verify if facility manager submitted an email of the most current Fleet report to readymixinspections@ncdot.gov.

- View and verify the certification of all on-site NCDOT Certified Concrete Field Technicians, if any. Ensure that technician certifications are active. List all names and required certification information in the table on the second page of the Audit Checklist. If marked as “N/A” provide an explanation in the Comments.

- View and verify the certification of all on-site NCDOT Concrete Batch Technicians. Ensure that technician certifications are active. List all names and required certification information in the table on the second page of the Audit Checklist. If marked as “N/A” provide an explanation in the Comments.

- View and verify that the facility is utilizing NCDOT approved mix designs. Hard copies must be on-site. If marked as “N/A” provide an explanation in the Comments.

- View and verify that the facility is utilizing approved materials (such as cement, fly ash, slag, aggregate, water, and admixtures, etc.) in accordance with the approved mix designs, ensuring conformity with the actual BOL for received materials.

- Verify calibration reports for the scales and actual stickers with dates, including smaller scales for the moisture tests. Scales shall be calibrated at least on a semiannual basis.

- Verify on-site whether the certified Batching Technician can perform moisture tests on Fine and Coarse aggregates, including calculations. Verify documentation related to the performance of moisture tests on fine and coarse aggregates. Verify that the moisture test equipment is in good and working condition. If marked as “N/A” provide an explanation in the Comments.

- Verify on-site that the certified Batching Technician has the ability to adjust moisture during the batching process. Review whether the batch tickets and/or operating process is acceptable.

- View on-site to ensure that the certified Batching Technician periodically performs the correlation of the moisture probe with actual moisture, if applicable, and has the ability to adjust moisture probe if needed. If marked as “N/A” provide an explanation in the Comments.

- View examples of associated NCDOT documentation, such as Form 903, Form 250, copies of batch weights tickets, etc., and verify that all those documents are fully completed for every NCDOT production of concrete. If marked as “N/A” provide an explanation in the Comments.

- Verify that current Admixture calibration report is on-site. Record inspection/expiration date on Audit Checklist form. Note: Admixture shall be calibrated at least on a semiannual basis.

# Verify that the annual water test report is on-site. Note: Ready Mixed Concrete facilities must undergo the water test a minimum of once per year. If marked as “N/A” provide an explanation in the Comments.

# Sample the water from the facility. Note: If the water sample was taken by the M&T inspector during the audit, after obtaining the test results, the M&T inspector shall provide a copy of that test report to the plant manager.

# Required Sampling:

# Top of the second page: M&T Inspector shall indicate if all materials for the concrete at the plant match BOL and all approved Mix designs.

- Cement – one gallon (plastic bag). Sample from the plant discharge end (not from the “test” bags).

- Fly Ash (or Slag) – one gallon (plastic bag). Sample from the plant discharge end (not from the “test” bags).

- Fine Aggregate – one bag (8 – 10 pounds). Sample from stockpiles or from the conveyor belt.

- Coarse Aggregate – #57 and #67 one bag (20 – 30 pounds); #78M one bag (10 – 15 pounds). Sample from stockpiles or from the conveyor belt.

- Water – ½ gallon (one wide mouth jar). Water shall be tested once per calendar year during annual audit and shall be obtained from the pipe that will feed water into the mixer.

- If using Well water, it shall be tested for 100% of facilities using this type of water for the concrete mixes.

- If using Public water, a sample is required only in the following counties: Beaufort, Bertie, Brunswick, Camden, Carteret, Chowan, Craven, Currituck, Dare, Gates, Hyde, New Hanover, Onslow, Pamlico, Pasquotank, Pender, Perquimans, Tyrell and Washington shall be tested a minimum of once per calendar year.

- For all Out-of-state facilities water shall be sampled and tested regardless of sources.

After receiving tests results of water, a copy of these records must be provided to the plant.

Samples should be submitted to Chemical and Physical Laboratories with appropriate sample cards. In a sample card for water shall be indicated: a) sources of water: Well or City; b) County; c) If it’s a new facility for NCDOT.

# Sample Prep and Submittal:

Sample containers shall be handled to avoid contamination during the sampling, log-in, and transportation process.

Sample cards shall be fixed to their corresponding sample container and transported to the appropriate laboratory for analysis.

Samples shall be entered utilizing the HiCAMS system - see Annual Facility Audit Field Manual for entry examples.

HiCAMS # for samples shall be provided in the Audit Checklist.

Documentation Submittal:

The completed (fill-in-the-blanks) “Ready Mixed Concrete Annual Facility Audit Checklist” shall be submitted as Word document to the email: ReadyMixInspections@ncdot.gov .  This document shall be submitted electronically.