
ASPHALT PAVEMENTS - SUPERPAVE:
	(6-19-12)
	605
	SP6 R01


Revise the 2012 Standard Specifications as follows:

Page 6-3, Article 605-7 APPLICATION RATES AND TEMPERATURES, replace this article, including Table 601-1, with the following:

Apply tack coat uniformly across the existing surface at target application rates shown in Table 605-1.
	TABLE 605-1
APPLICATION RATES FOR TACK COAT

	Existing Surface
	Target Rate (gal/sy)

	
	Emulsified Asphalt

	New Asphalt
	0.04 ± 0.01

	Oxidized or Milled Asphalt 
	0.06 ± 0.01

	Concrete
	0.08 ± 0.01


Apply tack coat at a temperature within the ranges shown in Table 605-2.  Tack coat shall not be overheated during storage, transport or at application.

	TABLE 605-2
APPLICATION TEMPERATURE FOR TACK COAT

	Asphalt Material
	Temperature Range

	Asphalt Binder, Grade PG 64-22
	350 - 400°F

	Emulsified Asphalt, Grade RS-1H
	130 - 160°F

	Emulsified Asphalt, Grade CRS-1
	130 - 160°F

	Emulsified Asphalt, Grade CRS-1H
	130 - 160°F

	Emulsified Asphalt, Grade HFMS-1
	130 - 160°F

	Emulsified Asphalt, Grade CRS-2
	130 - 160°F


Page 6-18, Article 610-1 DESCRIPTION, lines 40-41, delete the last sentence of the last paragraph.

Page 6-19, Subarticle 610-3(A) Mix Design-General, line 5, add the following as the first paragraph:
Warm mix asphalt (WMA) is allowed for use at the Contractor’s option in accordance with the NCDOT Approved Products List for WMA Technologies available at:

http://www.ncdot.org/doh/operations/materials/pdf/wma.pdf.
