
ASPHALT BINDER CONTENT OF ASPHALT PLANT MIXES:
	(11-21-00) (Rev. 7-17-12)
	609
	SP6 R15


The approximate asphalt binder content of the asphalt concrete plant mixtures used on this project will be as follows:

	Asphalt Concrete Base Course
	Type B 25.0__
	4.4%

	Asphalt Concrete Intermediate Course
	Type I 19.0__
	4.8%

	Asphalt Concrete Surface Course
	Type S 4.75A
	6.8%

	Asphalt Concrete Surface Course
	Type SA-1
	6.8%

	Asphalt Concrete Surface Course
	Type SF 9.5A
	6.7%

	Asphalt Concrete Surface Course
	Type S 9.5__
	6.0%

	Asphalt Concrete Surface Course
	Type S 12.5__
	5.6%


The actual asphalt binder content will be established during construction by the Engineer within the limits established in the 2012 Standard Specifications.
