ASPHALT CONCRETE SURFACE COURSE COMPACTION:
	(7-1-95) (Rev. 8-21-12)
	SP6 R49R


Compact the asphalt surface course on this project in accordance with Subarticle 610-9 of the 2012 Standard Specifications and the following provision:

Perform the first rolling with a steel wheel roller followed by rolling with a self-propelled pneumatic tired roller with the final rolling by a steel wheel roller.

