
OPEN GRADED ASPHALT FRICTION COURSE, PERMEABLE ASPHALT DRAINAGE COURSE, AND ULTRA-THIN BONDED WEARING COURSE:

	(4-17-12)
	609
	SP6 R62


When producing and constructing open graded asphalt friction course, permeable asphalt drainage course, and ultra-thin bonded wearing course revise the 2012 Standard Specifications as follows:

Page 6-10, Subarticle 609-6(B) Required Sampling and Testing Frequencies, delete the third paragraph and replace with the following:

Sample and test the completed mixture from each mix design per plant per year at the following minimum frequency during mix production:

	Accumulative Production Increment
	Number of Samples per Increment

	500 tons
	1


Page 6-10, Subarticle 609-6(C) Control Charts, delete the fourth paragraph and replace with the following:
Record the following data on the standardized control charts and in accordance with the requirements of Section 7.4 of the HMA/QMS Manual:

(a)
Aggregate Gradation Test Results:

1.
12.5 mm (Types P57 & FC-2 Mod. Only)

2.
9.5 mm (Excluding Type P57)

3.
4.75 mm 

4.
2.36 mm 

5.
0.075 mm Sieves

(b)
Binder Content, %, Pb
Page 6-11, Subarticle 609-6(D) Control Limits, Table 609-1 CONTROL LIMITS, replace with the following:

	TABLE 609-1

CONTROL LIMITS

	Mix Control Criteria
	Target Source
	Moving Average Limit
	Individual Limit

	12.5 mm Sieve (Types P57 & FC-2 Mod)
	JMF
	( 4.0
	( 8.0

	9.5 mm Sieve (Excluding Type P57)
	JMF
	( 4.0
	( 8.0

	4.75 mm Sieve
	JMF
	( 4.0
	( 8.0

	2.36 mm Sieve
	JMF
	( 4.0
	( 8.0

	0.075 mm Sieve
	JMF
	( 1.5
	( 2.5

	Binder Content
	JMF
	( 0.3
	( 0.7

	TSR (Ultra-thin Only)
	Min. Spec. Limit
	-
	- 15%


Page 6-12, Subarticle 609-6(F) Allowable Retesting for Mix Deficiencies, 
Table 609-2 RETEST LIMITS FOR MIX DEFICIENCIES, replace with the following:
	TABLE 609-2

RETEST LIMITS FOR MIX DEFICIENCIES

	Property
	Limit

	% Binder Content
	by more than ( 1.0%

	12.5 mm Sieve (Types P 57 & FC-2 Mod)
	by more than ( 9.0%

	9.5 mm Sieve (Excluding Type P 57)
	by more than ( 9.0%

	4.75 mm sieve
	by more than ( 9.0%

	2.36 mm sieve
	by more than ( 9.0%

	0.075 mm sieve
	by more than ( 3.0%

	TSR (Ultra-thin only)
	by more than -15% 
from Specification limit


Page 6-17, Subarticle 609-9(C) Limits of Precision, Table 609-3 LIMITS OF PRECISION FOR TEST RESULTS, replace with the following:
	TABLE 609-3

LIMITS OF PRECISION FOR TEST RESULTS

	Mix Property
	Limits of Precision

	12.5 mm Sieve (Types P 57 & FC-2 Mod. Only)
	( 6.0%

	9.5 mm Sieve (Excluding Type P 57)
	( 5.0%

	4.75 mm Sieve
	( 5.0%

	2.36 mm Sieve
	( 5.0%

	0.075 mm Sieve
	( 2.0%

	Asphalt Binder Content
	( 0.5%

	TSR (Ultra-thin HMA Only)
	( 15.0%


