
PREFORMED SCOUR HOLE WITH LEVEL SPREADER APRON:
	(10-15-02) (Rev. 10-20-09)
	410
	SP8 R105


Description

Construct and maintain preformed scour holes with spreader aprons at the locations shown on the plans and in accordance with the details in the plans.  Work includes excavation, shaping and maintaining the hole and apron, furnishing and placing filter fabric, rip rap (class as specified in the plans) and permanent soil reinforcement matting.

Materials

	Item
	
	Section

	Plain Rip Rap
	
	1042

	Filter Fabric
	
	1056


The permanent soil reinforcement matting shall be permanent erosion control reinforcement mat and shall be constructed of synthetic or a combination of coconut and synthetic fibers evenly distributed throughout the mat between a bottom UV stabilized netting and a heavy duty UV stabilized top net.  The matting shall be stitched together with UV stabilized polypropylene thread to form a permanent three dimensional structure.  The mat shall have the following minimum physical properties:

	Property
	Test Method
	Value
Unit

	Light Penetration
	ASTM D6567
	9 %

	Thickness
	ASTM D6525
	0.40 in

	Mass Per Unit Area
	ASTM D6566
	0.55 lb/sy

	Tensile Strength
	ASTM D6818
	385 lb/ft

	Elongation ( Maximum)
	ASTM D6818
	49 %

	Resiliency
	ASTM D1777
	>70 %

	UV Stability *
	ASTM 4355
	≥80 %

	Porosity (Permanent Net)
	ECTC Guidelines
	≥85 %

	Maximum Permissible Shear Stress (Vegetated)
	Performance Bench Test
	≥8.0 lb/ft2

	Maximum Allowable Velocity (Vegetated)
	Performance Bench Test
	≥16.0 ft/s


*ASTM D1682 Tensile Strength and % strength retention of material after 1,000 hours of exposure.

Submit a certification (Type 1, 2, or 3) from the manufacturer showing:

(A)
The chemical and physical properties of the mat used, and

(B)
Conformance of the mat with this specification.

Construction Methods

All areas to be protected with the mat shall be brought to final grade and seeded in accordance with Section 1660 of the 2012 Standard Specifications.  The surface of the soil shall be smooth, firm, stable and free of rocks, clods, roots or other obstructions that would prevent the mat from lying in direct contact with the soil surface.  Areas where the mat is to be placed will not need to be mulched.

Measurement and Payment

Preformed Scour Holes with Level Spreader Aprons will be measured and paid as the actual number incorporated into the completed and accepted work.  Such price and payment will be full compensation for all work covered by this provision.

Payment will be made under:

	Pay Item
	Pay Unit

	Preformed Scour Hole with Level Spreader Aprons
	Each


