
SELECT MATERIAL, CLASS III, TYPE 3:
	(1-17-12)
	1016, 1044
	SP10 R05


Revise the 2012 Standard Specifications as follows:

Page 10-39, Article 1016-3, CLASS III, add the following after line 14:
Type 3 Select Material

Type 3 select material is a natural or manufactured fine aggregate material meeting the following gradation requirements and as described in Sections 1005 and 1006:

	Percentage of Total by Weight Passing

	3/8"
	#4
	#8
	#16
	#30
	#50
	#100
	#200

	100
	95-100
	65-100
	35-95
	15-75
	5-35
	0-25
	0-8


Page 10-39, Article 1016-3, CLASS III, line 15, replace “either type” with “Type 1, Type 2 or Type 3”.
Page 10-62, Article 1044-1, line 36, delete the sentence and replace with the following:
Subdrain fine aggregate shall meet Class III select material, Type 1 or Type 3.

Page 10-63, Article 1044-2, line 2, delete the sentence and replace with the following:
Subdrain coarse aggregate shall meet Class V select material.

