OPEN GRADED ASPHALT FRICTION COURSE, PERMEABLE ASPHALT DRAINAGE COURSE, AND ULTRA-THIN BONDED WEARING COURSE:

| (4-17-12) | 609 | SP6 R62 |
| --- | --- | --- |

When producing and constructing open graded asphalt friction course, permeable asphalt drainage course, and ultra-thin bonded wearing course revise the 2012 Standard Specifications as follows:

Page 6-10, Subarticle 609-6(B) Required Sampling and Testing Frequencies, delete the third paragraph and replace with the following:

Sample and test the completed mixture from each mix design per plant per year at the following minimum frequency during mix production:

| Accumulative Production Increment | Number of Samples per Increment |
| --- | --- |
| 500 tons | 1 |

Page 6-10, Subarticle 609-6(C) Control Charts, delete the fourth paragraph and replace with the following:

Record the following data on the standardized control charts and in accordance with the requirements of Section 7.4 of the HMA/QMS Manual:

(a)	Aggregate Gradation Test Results:

1.	12.5 mm (Types P57 & FC-2 Mod. Only)

2.	9.5 mm (Excluding Type P57)

3.	4.75 mm

4.	2.36 mm

5.	0.075 mm Sieves

(b)	Binder Content, %, Pb

Page 6-11, Subarticle 609-6(D) Control Limits, Table 609-1 CONTROL LIMITS, replace with the following:

| TABLE 609-1 CONTROL LIMITS |
| --- |
| Mix Control Criteria | Target Source | Moving Average Limit | Individual Limit |
| 12.5 mm Sieve (Types P57 & FC-2 Mod) | JMF | ( 4.0 | ( 8.0 |
| 9.5 mm Sieve (Excluding Type P57) | JMF | ( 4.0 | ( 8.0 |
| 4.75 mm Sieve | JMF | ( 4.0 | ( 8.0 |
| 2.36 mm Sieve | JMF | ( 4.0 | ( 8.0 |
| 0.075 mm Sieve | JMF | ( 1.5 | ( 2.5 |
| Binder Content | JMF | ( 0.3 | ( 0.7 |
| TSR (Ultra-thin Only) | Min. Spec. Limit | - | - 15% |

Page 6-12, Subarticle 609-6(F) Allowable Retesting for Mix Deficiencies, 
Table 609-2 RETEST LIMITS FOR MIX DEFICIENCIES, replace with the following:

| TABLE 609-2 RETEST LIMITS FOR MIX DEFICIENCIES |
| --- |
| Property | Limit |
| % Binder Content | by more than ( 1.0% |
| 12.5 mm Sieve (Types P 57 & FC-2 Mod) | by more than ( 9.0% |
| 9.5 mm Sieve (Excluding Type P 57) | by more than ( 9.0% |
| 4.75 mm sieve | by more than ( 9.0% |
| 2.36 mm sieve | by more than ( 9.0% |
| 0.075 mm sieve | by more than ( 3.0% |
| TSR (Ultra-thin only) | by more than -15% from Specification limit |

Page 6-17, Subarticle 609-9(C) Limits of Precision, Table 609-3 LIMITS OF PRECISION FOR TEST RESULTS, replace with the following:

| TABLE 609-3 LIMITS OF PRECISION FOR TEST RESULTS |
| --- |
| Mix Property | Limits of Precision |
| 12.5 mm Sieve (Types P 57 & FC-2 Mod. Only) | ( 6.0% |
| 9.5 mm Sieve (Excluding Type P 57) | ( 5.0% |
| 4.75 mm Sieve | ( 5.0% |
| 2.36 mm Sieve | ( 5.0% |
| 0.075 mm Sieve | ( 2.0% |
| Asphalt Binder Content | ( 0.5% |
| TSR (Ultra-thin HMA Only) | ( 15.0% |