MATERIALS:

| (2-21-12) (Rev. 9-18-12) | 1005, 1081, 1092 | SP10 R01 |
| --- | --- | --- |

Revise the 2012 Standard Specifications as follows:

Page 10-5, Table 1000-1, REQUIREMENTS FOR CONCRETE, replace with the following:

| TABLE 1000-1 REQUIREMENTS FOR CONCRETE |
| --- |
| Class of Concrete | Min. Comp. Strength at 28 days | Maximum Water-Cement Ratio | Consistency Max. Slump | Cement Content |
|  |  | Air-Entrained Concrete | Non Air-Entrained Concrete | Vibrated | Non- Vibrated | Vibrated | Non- Vibrated |
|  |  | Rounded Aggre-gate | Angular Aggre-gate | Rounded Aggre-gate | Angular Aggre-gate |  |  | Min. | Max. | Min. | Max. |
| Units | psi |  |  |  |  | inch | inch | lb/cy | lb/cy | lb/cy | lb/cy |
| AA | 4,500 | 0.381 | 0.426 | - | - | 3.5 | - | 639 | 715 | - | - |
| AA Slip Form | 4,500 | 0.381 | 0.426 | - | - | 1.5 | - | 639 | 715 | - | - |
| Drilled Pier | 4,500 | - | - | 0.450 | 0.450 | - | 5-7 dry 7-9 wet | - | - | 640 | 800 |
| A | 3,000 | 0.488 | 0.532 | 0.550 | 0.594 | 3.5 | 4 | 564 | - | 602 | - |
| B | 2,500 | 0.488 | 0.567 | 0.559 | 0.630 | 2.5 | 4 | 508 | - | 545 | - |
| B Slip Formed | 2,500 | 0.488 | 0.567 | - | - | 1.5 | - | 508 | - | - | - |
| Sand Light-weight | 4,500 | - | 0.420 | - | - | 4 | - | 715 | - | - | - |
| Latex Modified | 3,000 7 day | 0.400 | 0.400 | - | - | 6 | - | 658 | - | - | - |
| Flowable Fill excavatable | 150 max. at 56 days | as needed | as needed | as needed | as needed | - | Flow-able | - | - | 40 | 100 |
| Flowable Fill non-excavatable | 125 | as needed | as needed | as needed | as needed | - | Flow-able | - | - | 100 | as needed |
| Pavement | 4,500 design, field 650 flexural, design only | 0.559 | 0.559 | - | - | 1.5 slip form 3.0 hand place | - | 526 | - | - | - |
| Precast | See Table 1077-1 | as needed | as needed | - | - | 6 | as needed | as needed | as needed | as needed | as needed |
| Prestress | per contract | See Table 1078-1 | See Table 1078-1 | - | - | 8 | - | 564 | as needed | - | - |

Page 10-23, Table 1005-1, AGGREGATE GRADATION-COARSE AGGREGATE, replace with the following:

|  | Light-weightC | ABC (M) | ABC | 9 | 14M | 78M | 67 | 6M | 57M | 57 | 5 | 467M | 4 | Std. Size # | Percentage of Total by Weight Passing | TABLE 1005-1 AGGREGATE GRADATION - COARSE AGGREGATE |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A. See Subarticle 1005-4(A). B. See Subarticle 1005-4(B). C. For Lightweight Aggregate used in Structural Concrete, see Subarticle 1014-2(E)(6). | - | - | - | - | - | - | - | - | - | - | - | 100 | 100 | 2" |  |  |
|  | - | 100 | 100 | - | - | - | - | - | 100 | 100 | 100 | 95-100 | 90-100 | 1 1/2" |  |  |
|  | - | 75- 100 | 75-97 | - | - | - | 100 | 100 | 95-100 | 95-100 | 90-100 | - | 20-55 | 1" |  |  |
|  | - | - | - | - | - | 100 | 90-100 | 90-100 | - | - | 20-55 | 35-70 | 0-15 | 3/4" |  |  |
|  | 100 | 45-79 | 55-80 | - | - | 98-100 | - | 20-55 | 25-45 | 25-60 | 0-10 | - | - | 1/2" |  |  |
|  | 80-100 | - | - | 100 | 100 | 75-100 | 20-55 | 0-20 | - | - | 0-5 | 0-30 | 0-5 | 3/8" |  |  |
|  | 5- 40 | 20-40 | 35-55 | 85-100 | 35-70 | 20-45 | 0-10 | 0-8 | 0-10 | 0-10 | - | 0-5 | - | #4 |  |  |
|  | 0-20 | - | - | 10-40 | 5-20 | 0-15 | 0-5 | - | 0-5 | 0-5 | - | - | - | #8 |  |  |
|  | - | 0- 25 | 25-45 | - | - | - | - | - | - | - | - | - | - | #10 |  |  |
|  | 0-10 | - | - | 0-10 | 0-8 | - | - | - | - | - | - | - | - | #16 |  |  |
|  | - | - | 14-30 | - | - | - | - | - | - | - | - | - | - | #40 |  |  |
|  | 0-2.5 | 0-12B | 4-12B | A | A | A | A | A | A | A | A | A | A | #200 |  |  |
|  | AST | Maintenance Stabilization | Aggregate Base Course, Aggregate Stabilization | AST | Asphalt Plant Mix, AST, Weep Hole Drains, Str. Concrete | Asphalt Plant Mix, AST, Str. Conc, Weep Hole Drains | AST, Str. Concrete, Asphalt Plant Mix | AST | AST, Concrete Pavement | AST, Str. Concrete, Shoulder Drain, Sediment Control Stone | AST, Sediment Control Stone | Asphalt Plant Mix | Asphalt Plant Mix | Remarks |  |  |

Page 10-126, Table 1078-1, REQUIREMENTS FOR CONCRETE, replace with the following:

| TABLE 1078-1 REQUIREMENTS FOR CONCRETE |
| --- |
| Property | 28 Day Design Compressive Strength 6,000 psi or less | 28 Day Design Compressive Strength greater than 6,000 psi |
| Maximum Water/Cementitious Material Ratio | 0.45 | 0.40 |
| Maximum Slump without HRWR | 3.5" | 3.5" |
| Maximum Slump with HRWR | 8" | 8" |
| Air Content (upon discharge into forms) | 5 + 2% | 5 + 2% |

Page 10-162, Subarticle 1081-1(A) Classifications, lines 4-7, delete the second and third sentences of the description for Type 3A.

Page 10-162, Subarticle 1081-1(B) Requirements, lines 26-30, replace the second paragraph with the following:

For epoxy resin systems used for embedding dowel bars, threaded rods, rebar, anchor bolts and other fixtures in hardened concrete, the manufacturer shall submit test results showing that the bonding system will obtain 125% of the specified required yield strength of the fixture.  Furnish certification that, for the particular bolt grade, diameter and embedment depth required, the anchor system will not fail by adhesive failure and that there is no movement of the anchor bolt.  For certification and anchorage, use 3,000 psi as the minimum Portland cement concrete compressive strength used in this test.  Use adhesives that meet Section 1081.

List the properties of the adhesive on the container and include density, minimum and maximum temperature application, setting time, shelf life, pot life, shear strength and compressive strength.

Page 10-169, Subarticle 1081-3(G) Anchor Bolt Adhesives, delete this subarticle.

Page 10-204, Subarticle 1092-2(A) Performance and Test Requirements, replace Table 1092-3 Minimum Coefficient of Retroreflection for NC Grade A with the following:

| TABLE 1092-3 MINIMUM COEFFICIENT OF RETROREFLECTION FOR NC GRADE A (Candelas Per Lux Per Square Meter) |
| --- |
| Observation Angle, degrees | Entrance Angle, degrees | White | Yellow | Green | Red | Blue | Fluorescent Yellow Green | Fluorescent Yellow |
| 0.2 | -4.0 | 525 | 395 | 52 | 95 | 30 | 420 | 315 |
| 0.2 | 30.0 | 215 | 162 | 22 | 43 | 10 | 170 | 130 |
| 0.5 | -4.0 | 310 | 230 | 31 | 56 | 18 | 245 | 185 |
| 0.5 | 30.0 | 135 | 100 | 14 | 27 | 6 | 110 | 81 |
| 1.0 | -4.0 | 120 | 60 | 8 | 16 | 3.6 | 64 | 48 |
| 1.0 | 30.0 | 45 | 34 | 4.5 | 9 | 2 | 36 | 27 |