**THERMOPLASTIC PAVEMENT MARKING MATERIAL – COLOR TESTING:**

|  |  |  |
| --- | --- | --- |
| 3-19-19 | 1087 | SP10 R05 |

Revise the *2018* *Standard Specifications* as follows:

**Pages 10-183 and 10-184, Subarticle 1087-7(D)(1)(b) Yellow,** lines 9-11, delete and replace with the following:

Obtain Color Values Y,x,y per ASTM E1349 using C/2° illuminant/observer.

Results shall be Y ≥ 45%, and x,y shall fall within PR#1 chart chromaticity limits.