**EXTRUDED THERMOPLASTIC PAVEMENT MARKING THICKNESS:**

|  |  |  |
| --- | --- | --- |
| 3-19-19 (Rev. 6-21-22) | 1205 | SP12 R05 |

Revise the *2018 Standard Specifications* as follows:

**Page 12-6, Subarticle 1205-4(A)(1) General, lines 5-8,** delete the second sentence andreplace with the following:

Use application equipment that provides multiple width settings ranging from 4 inches to 12 inches and multiple thickness settings to achieve the required thickness above the surface of the pavement as shown in Table 1205-3.

**Page 12-7, Table 1205-3, THICKNESS REQUIREMENTS FOR THERMOPLASTIC,** replace with the following:

|  |  |
| --- | --- |
| **TABLE 1205-3**  **MINIMUM THICKNESS REQUIREMENTS FOR THERMOPLASTIC** | |
| **Thickness** | **Location** |
| 240 mils | In-lane and shoulder-transverse pavement markings (rumble strips). May be placed in 2 passes. |
| 90 mils | Center lines, skip lines, transverse bands, mini-skip lines, characters, bike lane symbols, crosswalk lines, edge lines, gore lines, diagonals, and arrow symbols |