NON-TRACKING TACK COAT:

| (1-2-14)(Rev. 1-16-24) | 605 | SPD 6-100 |
| --- | --- | --- |

Revise the Standard Specifications as follows:

Page 6-4, SECTION 605 ASPHALT TACK COAT, line 30, after Section 605, add the following:

SECTION 606

NON-TRACKING ASPHALT TACK COAT

606-1 DESCRIPTION

Refer to Article 605-1.

Non-tracking tack coat will be required.  Notify the Engineer prior to using non-tracking tack coat.

606-2 MATERIALS

Use only “Non-tracking Asphalt Tack Coat” materials on the NCDOT APL.

Do not dilute or mix the non-tracking tack coat with water, solvents, or other materials before application.

606-3 WEATHER LIMITATIONS

Refer to Article 605-3.

606-4 SURFACE PREPARATION

Refer to Article 605-4.

606-5 ACCEPTANCE OF ASPHALT MATERIALS

Refer to Article 605-5.

606-6 APPLICATION EQUIPMENT

Refer to Article 605-6.

606-7 APPLICATION RATES AND TEMPERATURES

| TABLE 606-1 APPLICATION RATES FOR NON-TRACKING TACK COAT |  |
| --- | --- |
| Existing Surface | Target Rate (gal/sy) |
|  | Emulsified Asphalt |
| New Asphalt | 0.04 ± 0.01 |
| Oxidized or Milled Asphalt | 0.06 ± 0.01 |
| Concrete | 0.08 ± 0.01 |

Application temperatures shall be in accordance with manufacturer’s recommendations.  Non-tracking asphalt tack coat shall not be overheated.

606-8 APPLICATION OF TACK COAT

Refer to Article 605-8 except on Page 6-4, Article 605-8, line 5, replace second paragraph with the following:

If public traffic is being maintained, cover the non-tracking tack coat in the same day’s operation or provide continual lane closures until the tack is covered.  Due to non-tracking tack requiring heat to activate the adhesive properties, the application of temporary granular material will not be allowed.  If extended lane closures are required, applicable liquidated damages will apply.  To facilitate safe traffic conditions or for other reasons the Engineer may limit the application of non-tracking tack in advance of the paving operation.

606-9 MEASUREMENT AND PAYMENT

There will be no direct payment for the work covered by this section.

Page 6-21, Article 610-8, line 23, replace “Section 605” with “Sections 605 or 606”.

Page 6-37, Article 650-5, line 1, replace “Section 605” with “Sections 605 or 606”.

Page 6-38, Article 652-1, line 12, replace “Section 605” with “Sections 605 or 606”.