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Description

This works consists of furnishing and installing a polypropylene geotextile pavement fabric in accordance with the manufacturer’s recommendations and as directed by the Engineer.

Materials

The pavement fabric shall be furnished by an approved manufacturer of nonwoven polypropylene geotextiles.  A Certificate of Compliance from the manufacturer for the paving fabric used on the project shall be furnished to the Engineer.  The paving fabric shall be supplied in a protective cover or wrap that is capable of protecting the fabric from ultraviolet rays, abrasion, and water.  Use one of the following products:

Mirafi® MPV500 (TenCate Geosynthetics, (706) 693-2226, www.tencate.com ). 

PETROMAT 4599 (Propex Inc., (423) 899-0444 or (800) 621-1273, www.geotextile.com) 

US 100P (US Fabrics, (513) 271-6000, www.usfabricsinc.com )

Or Approved equal

Construction Methods

The Contractor shall follow the manufacturer’s recommendations for all aspects of the pavement fabric installation. 

The paving fabric shall be placed onto the asphalt cement with a minimum of wrinkles or folds before the asphalt can cool or lose its tackiness. Wrinkles severe enough to cause “folds” shall be slit and laid flat in the direction of paving operations. Broom the paving fabric in order to assist it in making intimate contact with the pavement surface. Any overlap of the paving fabric shall be minimized, although an overlap of 1 to 3 inches is recommended to ensure full closure of overlapping layers. Transverse joints shall be shingled (overlapped) in the direction of paving operations to prevent edge pick-up by the paver.

Stiff bristle brooms used to smooth, and scissors (or blades) used to cut the paving fabric shall be provided by the Installer. A pneumatic-tired roller may be needed in some cases to smooth paving fabric into the asphalt cement.

The asphalt distributor shall be suitably metered and capable of spraying the asphalt cement uniformly and at the prescribed application rate.  No drilling or skipping shall be permitted. Application of asphalt cement will be performed by truck-mounted distribution equipment whenever possible, with hand spraying kept to a minimum. The temperature of the asphalt cement shall be sufficiently high to permit a uniform spray pattern. The minimum recommended temperature for asphalt cement is 290oF, and shall not exceed 325oF at the contact surface.

Measurement and Payment

Pavement Fabric shall be measured and paid for in square yards of pavement fabric that has been installed and accepted.

Payment will be made under:

	Pay Item
	Pay Unit

	Pavement Fabric
	Square Yard



