ASPHALT CONCRETE SURFACE COURSE, TYPE SA-1:

| (4-17-12)(Rev. 1-16-24) | 610, 1012 | SPI 6-10 |
| --- | --- | --- |

Revise the Standard Specifications as follows:

Page 6-18, Table 610-2, AGGREGATE GRADATION CRITERIA, add the following:

|  | Mix Type (Nominal Max. Aggregate Size) |  |
| --- | --- | --- |
| Standard Sieves (mm) | 4.75 mm C |  |
|  | Min. | Max. |
| 50.0 | - | - |
| 37.5 | - | - |
| 25.0 | - | - |
| 19.0 | - | - |
| 12.5 | - | - |
| 9.50 | 100.0 |  |
| 4.75 | 90.0 | 100.0 |
| 2.36 | 65.0 | 90.0 |
| 1.18 | - | - |
| 0.600 | - | - |
| 0.300 | - | - |
| 0.150 | - | - |
| 0.075 | 4.0 | 8.0 |

C.  For Type SA-1, a minimum of 50% of the aggregate components shall be material manufactured from the crushing of stone.

Page 6-18, Table 610-3, MIX DESIGN CRITERIA, add the following:

| Mix Type | Design ESALs millions | Binder PG Grade | Compaction Levels |  | Max. Rut Depth (mm) | Volumetric Properties |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Gmm @ |  |  | VMA | VTM | VFA | %Gmm |
|  |  |  | Nini | Ndes |  | % Min. | % | Min.-Max. | @ Nini |
| SA-1F | <0.3 | 64 -22 | 6 | 50 | - | 20.0 | 7.0 - 15.0 | - | - |

F.  Mix Design Criteria for Type SA-1 may be modified subject to the approval of the Engineer.

Page 6-18, Table 610-3, MIX DESIGN CRITERIA, replace line 17, note E, with the following:

C.  TSR for Type SA-1, S4.75A, and Type B25.0C mixes is 80% minimum.

Page 6-20, Table 610-6, PLACEMENT TEMPERATURES FOR ASPHALT, replace “SF9.5A, S9.5B” in the “Asphalt Concrete Mix Type” column with “SA-1 S4.75A,  and S9.5B”.

Page 6-23, Table 610-7, DENSITY REQUIREMENTS, add the following:

| Mix Type | Minimum % of Gmm (Maximum Specific Gravity) |
| --- | --- |
| SA-1 | 85.0A, B |

Page 6-23, Table 610-7, DENSITY REQUIREMENTS, replace line 2, note A, with the following:

A. Compaction to the above specified density will be required when the SA-1 or S4.75A mix is applied at a rate of 100 lbs/sy or greater.

Page 6-23, Table 610-7, DENSITY REQUIREMENTS, add the following:

B.  All SA-1 pavement will be accepted for density in accordance with Article 105-3.

Page 6-31, Article 610-16, MEASUREMENT AND PAYMENT, add the following:

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Asphalt Concrete Surface Course, Type SA-1 | Ton |

Page 10-31, Subarticle 1012-1(B)(4), FLAT AND ELONGATED PIECES, replace line 44, “for Types SF9.5A and S9.5B.”, with the following:

“for Types SA-1, S4.75A and S9.5B.”

Page 10-32, Table 1012-1, AGGREGATE CONSENSUS PROPERTIES, add the following:

| Mix Type | Coarse Aggregate Angularity | Fine Aggregate Angularity % Minimum | Sand Equivalent % Minimum | Flat and Elongated 5 : 1 Ratio % Maximum |
| --- | --- | --- | --- | --- |
| Test Method | ASTM D5821 | AASHTO T 304 | AASHTO T 176 | ASTM D4791 |
| SA-1 | - | 40 | 40 | - |