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The use of Warm Mix Asphalt (WMA) is required on this project.  The JMF mix temperature shall be established at 275ºF or lower.  Assure temperature of the mixture immediately before discharge from the hauling vehicle is within a tolerance of ±25ºF of the specified JMF mix temperature. 

It is allowable at the beginning of a day’s production for the first few loads of WMA to be produced at a temperature up to 300 ºF for preheating of the plant and equipment.

