## ASPHALT PAVEMENTS (Maintenance Version):

| (1-2-14)(Rev. 7-15-25) | SPI 6-12 |
| --- | --- |

Construct asphalt pavements in accordance with Section 610 of the Standard Specifications and this special provision.

Provide and conduct quality control (QC) as specified in either Section 609 or under the special provision titled “Quality Management System for Asphalt Pavements (Maintenance Version)”, as applicable.  Design requirements for the various mix types shall meet the requirements of Table 610-2 and Table 610-3 of the Standard Specifications.  Surface testing of the completed pavement and performing all activities in accordance with the Department’s Asphalt Quality Management System (QMS) Manual is not required.  Warm mix asphalt (WMA) is not applicable to maintenance asphalt pavement processes nor as an additive.

Do not place plant mix base course or intermediate course unless it will be covered with surface course during the same calendar year or within 30 days of placement if the plant mix is placed in January or February, unless otherwise approved by the Engineer.  The second and fourth paragraph of Article 610-4 of the Standard Specifications do not apply.

Spread and finish in accordance with Article 610-8 of the Standard Specifications.  The use of pavers equipped with automatic control grade and cross-slope controls is recommended.

Compact in accordance with Article 610-9 of the Standard Specifications, except the third paragraph of this article does not apply and approval is not required for equipment used in compaction from the Engineer before use.

Surface requirements and acceptance shall be in accordance with Article 610-12 of the Standard Specifications except replace “2,500” with “500” in this article.

Final surface testing and acceptance in accordance with Article 610-13 of the Standard Specifications is not required.

Density acceptance shall be in accordance with the following paragraphs, instead of Article 610-14 of the Standard Specifications.

The Department will evaluate the asphalt pavement for density acceptance after the asphalt mix has been placed and compacted using the Contractor's QC test results, the Department's quality assurance (QA) test results (including verification samples) and by observation of the Contractor's density QC process in accordance with Section 609 of the Standard Specifications.  Minimum density requirements for all mixes will be as specified in the following table:

| DENSITY REQUIREMENTS |  |
| --- | --- |
| Mix Type | Minimum % Gmm (Maximum Specific Gravity) |
| S4.75A | 85.0 |
| S9.5B (2018) | 90.0 |
| S9.5C, S9.5D, I19.0C, B25.0C | 92.0 |

Density acceptance will be as provided herein.  Core sample densities will be determined using the average maximum specific gravity (Gmm) from the test(s) performed during the same day’s production.  The average Gmm in effect at the end of the same day's production will be used to evaluate acceptance.

The pavement will be accepted for density on a lot by lot basis.  A lot will consist of one day’s production of a given job mix formula on a contract.  As an exception, when multiple paving crews place asphalt simultaneously, a separate lot will be established for each paving crew.

Acceptance of all failing density lots constructed under this special provision will be made in accordance with Article 105-3 of the Standard Specifications.

Any reduction in pay due to failing density will be in addition to any reduction in pay due to failing mix property test results on the same mix.

Measurement and Payment

Asphalt Concrete ___________ Course, Type ______ for Maintenance will be paid at the contract unit price per ton that will be the actual number of tons of each type of hot mix asphalt pavement incorporated into the completed and accepted work in accordance with Article 106-7 of the Standard Specifications.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Asphalt Concrete ___________ Course, Type ______ for Maintenance | Ton |