NON-TRACKING TACK COAT:

| (1-2-14)(Rev. 1-16-24) | 605 | SPI 6-13A |
| --- | --- | --- |

Revise the Standard Specifications as follows:

Page 6-4, SECTION 605 ASPHALT TACK COAT, before line 30, after Section 605, add the following:

SECTION 606

NON-TRACKING ASPHALT TACK COAT

606-1 DESCRIPTION

Refer to Article 605-1.

Non-tracking tack coat will be required.  Notify the Engineer prior to using non-tracking tack coat.

606-2 MATERIALS

Use only products from the “Non-tracking Asphalt Tack Coat” materials on the NCDOT APL.

Use only an approved Hot Applied Tack for the open-graded asphalt friction course (OGAFC), if applicable.

Do not dilute or mix the non-tracking tack coat with water, solvents, or other materials before application.

606-3 WEATHER LIMITATIONS

Refer to Article 605-3 and Article 605-5 for OGAFC requirements.

606-4 SURFACE PREPARATION

Refer to Article 605-4.

606-5 ACCEPTANCE OF ASPHALT MATERIALS

Refer to Article 605-5.

606-6 APPLICATION EQUIPMENT

Refer to Article 605-6.

606-7 APPLICATION RATES AND TEMPERATURES

Target application rate for EMULSIFIED ASPHALT non-tracking tack shall be in accordance with Table 605-1, Application Rates for Tack Coat, contained elsewhere in this document, and if necessary adjust based on existing pavement conditions, milled surface, and manufacturer’s recommendations and approved by the Engineer.  Application temperatures shall be in accordance with manufacturer’s recommendations.  Non-tracking asphalt tack coat shall not be overheated.

Target application rate for HOT APPLIED TACK shall be 0.10 gal/sy and adjusted based on existing pavement conditions, milled surface, and manufacturer’s recommendations and approved by the Engineer.  Application temperatures shall be in accordance with manufacturer’s recommendations.  Non-tracking asphalt tack coat shall not be overheated.

606-8 APPLICATION OF TACK COAT

Refer to Article 605-8 except on Page 6-4, Article 605-8, line 5-9, replace second paragraph with the following:

If public traffic is being maintained, cover the non-tracking tack coat in the same day’s operation or provide continual lane closures until the tack is covered.  Due to non-tracking tack requiring heat to activate the adhesive properties, the application of temporary granular material will not be allowed.  If extended lane closures are required, applicable liquidated damages will apply.  To facilitate safe traffic conditions or for other reasons the Engineer may limit the application of non-tracking tack in advance of the paving operation.

606-9 MEASUREMENT AND PAYMENT

There will be no direct payment for the non-tracking tack coat and work covered by this section.

Payment at the contract unit prices for the various mix items covered by Sections 610, 650 and 654 will be full compensation for all work covered by this section.

Page 6-21, Article 610-8, line 23, replace “Section 605” with “Sections 605 or 606”.

Page 6-36, Article 650-5, line 13, replace “Section 605” with “Sections 605 or 606”.

Page 6-37, Article 652-1, line 26, replace “Section 605” with “Sections 605 or 606”.