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Revise the Standard Specifications as follows:

Page 6-4, SECTION 605 ASPHALT TACK COAT, before line 30, after Section 605, add the following:

SECTION 606
NON-TRACKING ASPHALT TACK COAT

606-1 DESCRIPTION

Refer to Article 605-1.

Non-tracking tack coat will be required.  Notify the Engineer prior to using non-tracking tack coat.

606-2 MATERIALS

Use only the Hot Applied Tack products from the “Non-tracking Asphalt Tack Coat” materials on the NCDOT APL.

Use only an approved Hot Applied Tack for the open-graded asphalt friction course (OGAFC) in lieu of Asphalt Binder, Grade PG-64-22 as stated in Article 650-5(A).

Do not dilute or mix the non-tracking tack coat with water, solvents, or other materials before application.

606-3 WEATHER LIMITATIONS 

Refer to Article 605-3 and Article 650-5 for OGAFC requirements.

606-4 SURFACE PREPARATION 

Refer to Article 605-4.

606-5 ACCEPTANCE OF ASPHALT MATERIALS 

Refer to Article 605-5.

606-6 APPLICATION EQUIPMENT 

Refer to Article 605-6.

606-7 APPLICATION RATES AND TEMPERATURES 

Target application rate for hot applied tack products shall be 0.10 gal/sy and adjusted based on existing pavement conditions, milled surface, and manufacturer’s recommendations and approved by the Engineer.  Application temperatures shall be in accordance with manufacturer’s recommendations.  Non-tracking asphalt tack coat shall not be overheated.

606-8 APPLICATION OF TACK COAT

Refer to Article 605-8 except on Page 6-4, Article 605-8, line 5-9, replace second paragraph with the following:

If public traffic is being maintained, cover the non-tracking tack coat in the same day’s operation or provide continual lane closures until the tack is covered.  Due to non-tracking tack requiring heat to activate the adhesive properties, the application of temporary granular material will not be allowed.  If extended lane closures are required, applicable liquidated damages will apply.  To facilitate safe traffic conditions or for other reasons the Engineer may limit the application of non-tracking tack in advance of the paving operation.

606-9 MEASUREMENT AND PAYMENT

There will be no direct payment for the non-tracking tack coat and work covered by this section.

Payment at the contract unit prices for the various mix items covered by Sections 610, 650 and 654 will be full compensation for all work covered by this section.

Page 6-21, Article 610-8, line 23, replace “Section 605” with “Sections 605 or 606”.

Page 6-36, Article 650-5, line 13, replace “Section 605” with “Sections 605 or 606”.

Page 6-37, Article 652-1, line 26, replace “Section 605” with “Sections 605 or 606”.

