6" JOINTED CONCRETE DRIVEWAY:

| (4-7-14)(Rev. 9-16-25) | 848 | SPI 7-20 |
| --- | --- | --- |

Description

Construct 6" jointed concrete driveway in accordance with Section 848 of the Standard Specifications, the plans, this special provision and as directed by the Engineer.

Materials

Use materials meeting the requirements of Article 848-2 of the Standard Specifications.

Welded wire reinforcement shall meet the requirements of Section 1070 of the Standard Specifications.

Construction Methods

Construct jointed concrete driveway consisting of 6 inches of Portland cement concrete pavement reinforced with steel welded wire reinforcement, size 4x4 W2.9XW2.9.  A heavier wire reinforcement, approved by the Engineer, may be used at no additional cost to the Department.  Position the steel welded wire reinforcement at mid-depth of the slab.  No later than 24 hours after concrete placement, saw cut contraction joints 1/8 inches wide and 2 inches deep at a spacing approximately equal to the slab width, but no more than 15 feet in each direction, or as directed by the Engineer.

Measurement and Payment

6" Jointed Concrete Driveway will be measured and paid in square yards, measured along the surface of the completed and accepted work. Such price includes, but is not limited to, excavating and backfilling, sawing the existing driveway, furnishing and placing wire mesh reinforcement and concrete, and constructing and sealing joints.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| 6" Jointed Concrete Driveway | Square Yards |