GROOVING EXISTING CONCRETE PAVEMENT:
	(12-15-09)
	SPI 8-26



Description

Perform the work covered by this provision including but not limited to longitudinal grooving the surface of existing Portland cement concrete pavement at the locations and of the dimensions shown on the plans and in accordance with the contract documents, selecting diamond tipped saw blades and configuration of cutting head; continual removal of residual slurry from pavement and proper disposal off-site; furnishing all labor, materials, supplies, tools, equipment and incidentals as necessary.  

Equipment

Furnish equipment that is power-driven, self-propelled and equipped with diamond blades specifically designed to groove Portland cement concrete pavement.  

Utilize equipment that does not cause ravels; aggregate fracture; spalls or disturbance to the longitudinal or transverse joints; or damage and strain to the underlying surface of the pavement.  Should any of the above problems occur immediately suspend operations.

Provide vacuuming equipment to continuously remove slurry residue and excess water from the pavement as part of the grooving operation.  
Provide grinder with the following features:

Depth control device that will detect and respond to variations in the concrete surface
Adjustable cutting head height to maintain the depth of groove specified
Diamond tipped grooving blades that are 0.095±0.003 inches wide and spaced ¾ inches on centers 
Devices to control alignment

Construction Requirements

Begin and end the grooved areas at lines normal to the pavement center line and centered within the lane width.  Groove the surface of the pavement without causing excessive raveling of the joints, and without cracking or fracturing the aggregates.

Provide grooves cut to not less than 1/8 inch or more than 1/4 inch deep.  Provide grooves on bridge decks cut to not less than 1/8 inch or more than 3/16 inches deep.

The actual grooved area of any selected 2 foot by 100 foot longitudinal area of pavement specified to be grooved shall not be less than 95% of the selected area.  Any portion of the selected area not grooved, shall be due only to irregularities in the pavement surface and for no other reason.

Do not allow slurry from the grooving operations to accumulate on adjacent lanes to the extent that it would create slippery or hazardous conditions.  Do not allow the slurry material to flow into a travel lane occupied by traffic or into any drainage facility.  Continuously remove residue resulting from grooving operations from pavement surfaces.  Immediately leave pavements in a washed clean condition, free of all slipperiness from the slurry and other debris.  Do not dispose of slurry in the existing drains or on the slopes of the roadway.  Place all debris and surplus material removed from the grooving operations in a truck or other conveyance designed to prevent loss of any liquid when being hauled to the disposal site; remove from the project and dispose of properly.

Measurement and Payment

Grooving Existing Concrete Pavement will be measured and paid for in square yards of completed and accepted work.  Such price and payment will include water, removal and proper disposal of residue off-site, and for all labor, tools, materials, equipment and incidentals necessary to complete the work.

Payment will be made under:

	Pay Item
	Pay Unit

	Grooving  Existing Concrete Pavement
	Square Yard



