
CONCRETE TRUCK APRON, ROLLED CONCRETE CURB AND CURB AND GUTTER (MODIFIED):
	  (1-21-24)(Rev. 10-20-26)
	SP8 R05



Description

Construct the concrete truck apron in accordance with the appliable requirements of Division 7 of the Standard Specifications, the plans and this special provision.

Construct rolled concrete curb and concrete curb and gutter (modified) in accordance with Section 846 of the Standard Specifications, the Roadway Standard Drawings No. 846.01 as modified by the typical section in the plans and this special provision. 

Materials

[bookmark: _Hlk205981947][bookmark: _Hlk205981959][bookmark: _Hlk205982000]Use materials meeting the applicable requirements of Article 710-2 and Section 700 of the Standard Specifications except all rolled concrete curb and curb and gutter (modified) in the roundabout and the concrete truck apron respectively shall be Class AA.

Portland cement concrete shall meet the requirements of Section 1000 of the Standard Specifications.

Wire welded reinforcement shall meet the requirements of Section 1070 of the Standard Specifications.

Construction Methods

Construct concrete truck apron in accordance with the applicable requirements of Article 710-3 and Section 700 of the Standard Specifications, the plans and as directed by the Engineer.  Final surface testing is not required. 

Construct rolled concrete curb and concrete curb and gutter (modified) and in accordance with Article 846-3 of the Standard Specifications, the plans and as directed by the Engineer.

Construct concrete truck apron consisting of Portland cement concrete pavement reinforced with steel welded wire reinforcement, size 4x4 W5.5XW5.5 or 6x6 W8.5X8.5.  A heavier wire reinforcement, approved by the Engineer, may be used at no additional cost to the Department.  Position the steel welded wire reinforcement at mid-depth of the slab.  Joints for the concrete truck apron shall be radial.  Expansion joint spacing shall not exceed 60 feet and contraction joint spacing shall not exceed 15 feet on centers, measured at the outside edge of the apron, or as directed by the Engineer.

Measurement and Payment

___" Concrete Truck Apron will be measured and paid for in square yards, measured along the surface of the completed and accepted work.  Such price and payment will be full compensation for all work of constructing the truck apron, including but not limited to excavating and backfilling, furnishing and placing concrete, and constructing joints.

2' 6" Concrete Curb and Gutter (Modified) will be measured and paid for in accordance with Article 846-4 of the Standard Specifications.

___" Rolled Concrete Curb will be measured and paid for in accordance with Article 846-4 of the Standard Specifications.

Payment will be made under:

	Pay Item
	Pay Unit

	___" Concrete Truck Apron
	Square Yard

	2' 6" Concrete Curb and Gutter (Modified)
	Linear Foot



