**WATTLE DEVICES:**

|  |  |  |
| --- | --- | --- |
|  (1-1-24) | 1642 | SP16 R01 |

**Page 16-23, Subarticle 1642-2(B) Wattle,** lines 10-12,delete andreplace with the following:

**(B) Wattle and Wattle Barrier**

Wattles shall meet Table 1642-1.

|  |
| --- |
| **TABLE 1642-1** **100% CURLED WOOD (EXCELSIOR) FIBERS - WATTLE** |
| **Property** | **Property Value** |
| Minimum Diameter | 12 inches |
| Minimum Density | 2.5 pcf +/- 10% |
| Net Material | Synthetic |
| Net Openings | 1 inch x 1 inch |
| Net Configuration | Totally Encased |
| Minimum Weight | 20 lb +/- 10% per 10 foot length |

Coir Fiber Wattles shall meet Table 1642-2.

|  |
| --- |
| **TABLE 1642-2** **100% COIR (COCONUT) FIBERS WATTLE** |
| **Property** | **Property Value** |
| Minimum Diameter | 12 inches |
| Minimum Density | 3.5 pcf +/- 10% |
| Net Material | Coir Fiber |
| Net Openings | 2 inch x 2 inch |
| Net Strength | 90 lb |
| Minimum Weight | 2.6 pcf +/- 10% |

Wattle Barriers shall meet Table 1642-3.

|  |
| --- |
| **TABLE 1642-3** **100% CURLED WOOD (EXCELSIOR) FIBERS – WATTLE BARRIER** |
| **Property** | **Property Value** |
| Minimum Diameter | 18 inches |
| Minimum Density | 2.9 pcf +/- 10% |
| Net Material | Synthetic |
| Net Openings | 1 inch x 1 inch |
| Net Configuration | Totally Encased |
| Minimum Weight | 5 pcf +/- 10% |

Coir Fiber Wattle Barriers shall meet Table 1642-4.

|  |
| --- |
| **TABLE 1642-4** **100% COIR (COCONUT) FIBERS WATTLE BARRIER** |
| **Property** | **Property Value** |
| Minimum Diameter | 18 inches |
| Minimum Density | 5 pcf +/- 10% |
| Net Material | Coir Fiber |
| Net Openings | 2 inch x 2 inch |
| Net Strength | 90 lb |
| Minimum Weight | 10 pcf +/- 10% |

**Pages 16-24 & 16-25, Article 1642-5 MEASUREMENT AND PAYMENT,** lines 42-47 & lines 1-2,delete andreplace with the following:

*Wattle* will be measured and paid for by the actual number of linear feet of wattles which are installed and accepted. Such price and payment will be full compensation for all work covered by this section, including, but not limited to, furnishing all materials, labor, equipment and incidentals necessary to install the *Wattle*.

*Coir Fiber Wattles* will be measured and paid for by the actual number of linear feet of coir fiber wattles which are installed and accepted. Such price and payment will be full compensation for all work covered by this section, including, but not limited to, furnishing all materials, labor, equipment and incidentals necessary to install the *Coir Fiber Wattles*.

*Wattle Barrier* will be measured and paid as the actual number of linear feet of wattle barrier installed and accepted. Such price and payment will be full compensation for all work covered by this provision, including, but not limited to, furnishing all materials, labor, equipment and incidentals necessary to install the *Wattle Barrier*.

*Coir Fiber Wattle Barrier* will be measured and paid as the actual number of linear feet of coir fiber wattle barrier installed and accepted. Such price and payment will be full compensation for all work covered by this provision, including, but not limited to, furnishing all materials, labor, equipment and incidentals necessary to install the *Coir Fiber Wattle Barrier*.

**Page 16-25, Article 1642-5 MEASUREMENT AND PAYMENT,** after line 9,delete andreplace “\_\_\_ Wattle Check” with “Wattle”.

**Page 16-25, Article 1642-5 MEASUREMENT AND PAYMENT,** after line 9,delete andreplace “\_\_\_ Wattle Barrier” with “Wattle Barrier”.

**Page 16-25, Article 1642-5 MEASUREMENT AND PAYMENT,** after line 9,add the following:

|  |  |
| --- | --- |
| **Pay Item** | **Pay Unit** |
| Coir Fiber Wattle | Linear Foot |
| Coir Fiber Wattle Barrier | Linear Foot |