ASPHALT CONCRETE SURFACE COURSE, TYPE S4.75A:

| (2-21-12) (Rev. 6-19-12) | 610, 1012 | SPD 6-200 |
| --- | --- | --- |

Revise the 2012 Standard Specifications as follows:

Page 6-21, Table 610-2, SUPERPAVE AGGREGATE GRADATION CRITERIA, add the following:

| Standard Sieves (mm) | Mix Type (Nominal Max. Aggregate Size) |  |
| --- | --- | --- |
|  | 4.75 mm |  |
|  | Min. | Max. |
| 50.0 | - | - |
| 37.5 | - | - |
| 25.0 | - | - |
| 19.0 | - | - |
| 12.5 | 100.0 | - |
| 9.50 | 95.0 | 100.0 |
| 4.75 | 90.0 | 100.0 |
| 2.36 | - | - |
| 1.18 | 30.0 | 60.0 |
| 0.600 | - | - |
| 0.300 | - | - |
| 0.150 | - | - |
| 0.075 | 6.0 | 12.0 |

Page 6-22, Table 610-3, SUPERPAVE MIX DESIGN CRITERIA, add the following:

| Mix Type | Design ESALs millions | Binder PG Grade | Compaction Levels |  | Max. Rut Depth (mm) | Volumetric Properties |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Gmm @ |  |  | VMA | VTM | VFA | %Gmm |
|  |  |  | Nini | Ndes |  | % Min. | % | Min. - Max. | @ Nini |
| S4.75A | For Pilot Program: < 1 | 64-22 | 6 | 50 | - | 16.0 | 4.0 - 6.0 | 65 - 80 | ≤ 91.5 |

Page 6-22, Table 610-3, SUPERPAVE MIX DESIGN CRITERIA, replace line 4, note C, with the following:

C.  TSR for Type S4.75A and Type B25.0 mixes is 80% minimum.

Page 6-23, Table 610-5, PLACEMENT TEMPERATURES FOR ASPHALT, replace “SF9.5A, S9.5B” in the “Asphalt Concrete Mix Type” column with “S4.75A, SF9.5A and S9.5B”.

Page 6-28, Table 610-6, SUPERPAVE DENSITY REQUIREMENTS, add the following:

| Superpave Mix Type | Minimum % of Gmm (Maximum Specific Gravity) |
| --- | --- |
| S4.75A | 85.0(a) |

(a)  Compaction to the above specified density will be required when the S4.75A mix is applied at a rate of 100 lb/sy or greater.

Page 6-37, Article 610-16, MEASUREMENT AND PAYMENT, add the following:

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Asphalt Concrete Surface Course, Type S4.75A | Ton |

Page 10-26, Subarticle 1012-1(B)(4), FLAT AND ELONGATED PIECES, replace line 44, “for Types SF9.5A and S9.5B.”, with the following:

“for Types S4.75A, SF9.5A and S9.5B.”

Page 10-27, Table 1012-1, AGGREGATE CONSENSUS PROPERTIES, add the following:

| Mix Type | Coarse Aggregate Angularity | Fine Aggregate Angularity % Minimum | Sand Equivalent % Minimum | Flat & Elongated 5 : 1 Ratio % Maximum |
| --- | --- | --- | --- | --- |
| Test Method | ASTM D 5821 | AASHTO T 304 | AASHTO T 176 | ASTM D 4791 |
| S4.75A | - | 40 | 40 | - |