PAINTED GALVANIZED STEEL BEAM GUARDRAIL:

| (9-19-06) (Rev 4-19-11) |  | SPD 8-800 |
| --- | --- | --- |

Description

Install painted galvanized steel beam guardrail and anchor units at locations shown on the plans.

Materials

Refer to Division 10 of the 2018 Standard Specifications.

| Item | Section |
| --- | --- |
| Galvanizing | 1076 |  |
| Reflective Sheeting | 1088-3 |  |

Guardrail materials shall meet the requirements of Section 1046 of the Standard Specifications except that guardrail materials shall not be water quenched or treated with chromate conversion coatings.

For painted Guardrail Anchor Units, Type 350, the Contractor may at his option, furnish any one of the following guardrail anchor units or an approved equal.

Guardrail anchor unit (ET-2000) as manufactured by:

Trinity Industries, Inc.

2525 N. Stemmons Freeway

Dallas, Texas  75207

Telephone:  800-644-7976

The guardrail anchor unit (SKT 350) as manufactured by:

Road Systems, Inc.

3616 Old Howard County Airport

Big Spring, Texas 79720

Telephone:  915-263-2435

Prior to installation the Contractor shall submit the following to the Engineer:

(A)	FHWA acceptance letter for each guardrail anchor unit certifying it meets the requirements of NCHRP Report 350, Test Level 3, in accordance with Article 106-2 of the Standard Specifications.

(B)	Certified working drawings and assembling instructions from the manufacturer for each guardrail anchor unit in accordance with Article 105-2 of the Standard Specifications.

No modifications shall be made to the guardrail anchor unit without the express written permission from the manufacturer.

Painting shall be performed in accordance with the requirements of Section 1080 and Section 442 of the Standard Specifications using System 4 as modified herein.

| System 4 (Modified) Acrylic Primer and Top Coats |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Coat |  | Material |  | Mils Dry/Wet Film Thickness |  | Mils Dry/Wet Film Thickness |  |
|  |  |  |  | Minimum |  | Maximum |  |
| Primer | 1080-12 White |  | 3.0 DFT |  | 5.0 DFT |  |
| Stripe | 1080-12 Brown |  | 4.0 WFT |  | 7.0 WFT |  |
| Topcoat | 1080-12 Brown |  | 2.0 DFT |  | 4.0 DFT |  |
| Total |  |  | 5.0 DFT |  | 9.0 DFT |  |

Construction Methods

(A)	Preparation of Galvanized Beams and Hardware for Painting

Perform surface smoothing by removing or cleaning all zinc high spots, such as metal drip line, by hand or power tools in accordance with SSPC SP 2 or 3.  Level zinc material flush with the surrounding plane without removing the base coating.

Abrasive sweep blasting shall be performed in accordance with Section 5.4.1 of ASTM D6386.  This section also provides a description of the abrasive blast material to be used.  The material and technique used will provide a stripping action to remove corrosion products and to provide a rough surface profile while leaving base zinc layers intact.

All surfaces of the blasted beams and hardware shall be blown down with clean compressed air to provide a clean, dry surface for additional coating to be applied.

All surfaces shall be free of visible zinc oxides or zinc hydroxides.

(B)	(1)	Certification

Only SSPC QP-3 certified contractor shall shop paint guardrail material.

(2)	Shop Paint

Galvanized guardrail beams, both front and back, posts, anchor units and hardware shall be shop painted within 8 hours after surface preparation except paint bolt heads after installation.

(C)	Repair of Damaged Coating

Repair damage occurring to the galvanized portion of the coating during shipment or installation in accordance with Articles 1076-6 and 1080-9 of the Standard Specifications.  Repair damage occurring to the painted portion of the coating during shipment or installation by applying 4.0 to 7.0 wet mils of topcoat with a brush or roller and feather or taper this to be level with the surrounding areas.

(D)	Guardrail Installation

Install guardrail in accordance with Section 862, details in the plans, and details and assembling instructions furnished by the manufacturer.  Guardrail end delineation shall be applied to the entire end section of all approach and trailing end sections.

(E)	Guardrail End Delineation

Guardrail end delineation is required on all approach and trailing end sections for both temporary and permanent installations.  Guardrail end delineation consists of yellow reflective sheeting applied to the entire end section of the guardrail in accordance with Article 1088-3 of the Standard Specifications and is incidental to the cost of the guardrail anchor unit.

Measurement and Payment

Painted Steel Beam Guardrail and Painted Steel Beam Guardrail, Shop Curved will be measured and paid in accordance with Article 862-6 of the Standard Specifications.

Painted Guardrail Anchor Units, Type ____ will be measured and paid in accordance with Article 862-6 of the Standard Specifications.

Painted Steel Beam Guardrail Terminal Sections and Painted Additional Guardrail Posts will be measured and paid in accordance with Article 862-6 of the Standard Specifications.

Such price and payment includes, but is not limited to, furnishing and erecting posts, offset blocks, rail, terminal sections, miscellaneous hardware, and all other materials, field curving and shop curving of the rail; excavation; furnishing and installing additional guardrail posts and additional offset blocks; backfilling; fabrication; welding; painting, galvanizing; furnishing and installing guardrail delineators and end delineation.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Painted Galvanized Steel Beam Guardrail | Linear Foot |
| Painted Galvanized Steel Beam Guardrail, Shop Curved | Linear Foot |
| Painted Galvanized Guardrail Anchor Units, Type ____ | Each |
| Painted Galvanized Guardrail Terminal Section | Each |
| Painted Galvanized Additional Guardrail Posts | Each |