**ASPHALT BINDER CONTENT OF ASPHALT PLANT MIXES:**

|  |  |  |
| --- | --- | --- |
| (11-21-00) (Rev. 7-17-12) | 609 | SP6 R15 |

The approximate asphalt binder content of the asphalt concrete plant mixtures used on this project will be as follows:

|  |  |  |
| --- | --- | --- |
| Asphalt Concrete Base Course | Type B 25.0\_\_ | 4.4% |
| Asphalt Concrete Intermediate Course | Type I 19.0\_\_ | 4.8% |
| Asphalt Concrete Surface Course | Type S 4.75A | 6.8% |
| Asphalt Concrete Surface Course | Type SA-1 | 6.8% |
| Asphalt Concrete Surface Course | Type SF 9.5A | 6.7% |
| Asphalt Concrete Surface Course | Type S 9.5\_\_ | 6.0% |
| Asphalt Concrete Surface Course | Type S 12.5\_\_ | 5.6% |

The actual asphalt binder content will be established during construction by the Engineer within the limits established in the *2012* *Standard Specifications.*