# Painting Existing structure	(12-5-12)

## Description

This work shall consist of furnishing all labor, equipment, and materials necessary to clean and paint the structural steel of the existing bridge.  Work includes: removal, containment and disposal of the existing paint system; preparation of the surface to be painted and applying the new paint system; a containment enclosure; and any incidentals necessary to complete the project as specified and shown on the plans.

## Certification

The existing paint systems include toxic substances such as red lead oxide, which are considered hazardous if improperly removed.  The contractor shall be currently SSPC QP 2, Category A certified, and have successfully completed lead paint removal and field painting on similar structures within 18 months prior to this bid.

The apparent low bidder shall submit a list of projects for which QP 2 work was performed within the last 18 months including owner contact information and submit to the Assistant State Structures Engineer (Operations) a “Lead Abatement Affidavit” by 12:00 noon of the third day following the opening of bids.  This form may be downloaded from:  http://www.ncdot.gov/projects/ncbridges/#stats.

The Engineer will evaluate the work history to verify all lead abatement work was completed in accordance with contract specifications, free of citation from safety or environmental agencies.  Lead abatement work shall include, but not be limited to:  abrasive blasting; waste handling, storage and disposal; worker safety during lead abatement activities (fall protection, PPE, etc.); and containment.  This requirement is in addition to the contractor pre-qualification requirements covered by Article 102-2 of the 2012 Standard Specifications.

## Twelve-Month Observation Period

The Contractor maintains responsibility for the coating system for a 12 month observation period beginning upon the satisfactory completion of all the work required in the plans or as directed by the Engineer.  The Contractor shall guarantee the coating system under the payment and performance bond (refer to Article 109-10 of the 2012 Standard Specifications).  To successfully complete the observation period, the coating system shall meet the following requirements after 12 months service:

(A)	No visible rust, contamination or application defect is observed in any coated area.

(B)	Painted surfaces have a uniform color and gloss.

(C)	Painted surfaces have an adhesion that meets an ASTM D3359, 3A rating.

Final acceptance is made only after the paint system meets the above requirements.

## Submittals

Submit all of the following to the Engineer for review and approval before scheduling the pre-construction meeting.  Allow at least 2 weeks for the review process.

(A)	Work schedule which shall be kept up to date, with a copy of the revised schedule being provided to the Engineer in a timely manner,

(B)	Containment Drawings in accordance with SSPC Guide 6, Class 2A sealed by a Professional Engineer licensed by the State of North Carolina,

(C)	Bridge wash water sampling and disposal plan,

(D)		Subcontractor identification,

(E)	Lighting plan for night work in accordance with Section 1413 of the 2012 Standard Specifications,

(F)	Traffic control plan with NCDOT certified supervisors, flaggers and traffic control devices,

(G)	Health and safety plan addressing at least the required topics as specified by the SSPC QP 1 and QP 2 program and including hazard communication, respiratory health, emergency procedures, and local hospital and treatment facilities with directions and phone numbers, disciplinary criteria for workers who violate the plan and accident investigation.  The plan shall address the following:  hazardous materials, personal protective equipment, general health and safety, occupational health and environmental controls, fire protection and prevention, signs signals, and barricades, materials handling, storage, use, and disposal, hand and power tools, welding and cutting, electrical, scaffolds, fall protection, cranes, derricks, hoists, elevators, and conveyors, ladders, toxic and hazardous substances, airless injection and HPWJ.

(H)	Provide the Engineer a letter of certification that all employees performing work on the project have blood lead levels that are below the OSHA action level.

(I)	Provide the Engineer with Competent Person qualifications and summary of work experience.

(J)	Environmental Compliance Plan

(K)	Quality Control Plan (Project Specific) with quality control qualifications and summary of work experience.

(L)	Bridge and Public Protection Plan (Overspray, Utilities, etc. - Project/Task Specific)

(M)	Abrasive Blast Media

(1)	Product Data Sheet

(2)	Blast Media Test Reports in accordance with Article 1080-13 of the 2012 Standard Specification.

(N)	Coating Material

(1)	NCDOT HICAMS Test Reports (testing performed by NCDOT Materials and Tests Unit),

(2)	Product Data Sheets,

(3)	Material Safety Data Sheets,

(4)	Product Specific Repair Procedures, and

(5)	Acceptance letters from paint manufacturer’s for work practices that conflict with Project Special Provisions and/or paint manufactures product data sheets.

## Pre-Construction Meeting

Submittals shall be reviewed and approved by the Engineer prior to scheduling the pre-construction meeting.  Allow no less than 2 weeks for a review process.  When requesting a
pre-construction meeting, contact the Engineer at least 7 working days in advance of the desired pre-construction date.  The contractor’s project supervisor, Competent person, quality control personnel and certified traffic control supervisor shall be in attendance at the pre-construction meeting in order for the Contractor and NCDOT team to establish responsibilities for various personnel during project duration and to establish realistic timeframes for problem escalation.

## Containment Plan

No work begins until the Contractor furnishes the Engineer with a containment plan for surface preparation and coating operations and the Engineer reviews and approves, in writing, the acceptability of said plan.  Allow a minimum of two weeks for review of the plan.  Such plan shall meet or exceed the requirements of Class 2A containment in accordance with SSPC Guide 6.  Enclosure drawings and loads supported by the structure shall be prepared, signed and sealed by a Professional Engineer licensed by the State of North Carolina.

In the containment plan describe how debris is contained and collected.  Describe the type of tarpaulin, bracing materials and the maximum designed wind load.  Describe the dust collection system and how a negative pressure of 0.03 inches of water column is maintained inside the enclosure while blasting operations are being conducted.  Describe how the airflow inside the containment structure is designed to meet all applicable OSHA Standards.  Describe how water run-off from rain will be routed by or through the enclosure.  Describe how wash water will be contained and paint chips separated.  Describe what physical containment will be provided during painting application to protect the public and areas not to be painted.

## Wash Water Sampling and Disposal Plan

No work begins until the Contractor furnishes the Engineer with a containment plan for surface preparation and coating operations and the Engineer reviews and approves in writing said plan.  All wash water shall be collected and sampled prior to disposal.  Representative sampling and testing methodology shall conform to 15A NCAC 02B.0103, “Analytical Procedures”.  Wash water shall be tested for pollutants listed in 15A NCAC 02B.0211(3), 15A NCAC 02T.0505(b)(1) and 15A NCAC 2T.0905(h).  Depending on the test results, wash water disposal methods shall be described in the disposal plan.  Wash water shall be disposed of in accordance with all current Federal and State regulations.  See link for NCDOT Guidelines for Managing Bridge Wash Water:  http://www.ncdot.gov/projects/ncbridges/#stats.

## Waste Handling of Paint and Abrasives

Comply with all Federal, State and local regulations.  Failure to comply with the regulations could result in fines and loss of qualified status with NCDOT.

Comply with the Resource Conservation and Recovery Act (RCRA - 40 CFR 261 - 265) and the Occupational Safety and Health Act (OSHA - 29 CFR 1910 - 1926) regulations for employee training, and for the handling, storage, labeling, recordkeeping, reporting, inspections and disposal of all hazardous waste generated during paint removal.

A summary of Generator Requirements is available at the above NCDOT web link which cites the specific regulations for each Generator category.  Quantities of waste by weight and dates of waste generation shall be recorded.  Waste stored at the project site shall be properly labeled. All waste, hazardous or non-hazardous, requires numbered shipping manifests.

The North Carolina Department of Environment and Natural Resources (NCDENR) have adopted RCRA as the North Carolina Hazardous Waste Management Rules and are responsible for enforcement.  The “Hazardous Waste Compliance Manual for Generators of Hazardous Waste” is published by the Compliance Branch of the Division of Waste Management of NCDENR, and can be found at:  http://portal.ncdenr.org/web/wm/hw/rules.

Use a company from the below list of approved waste management companies.  Immediately after award of the contract, arrange for waste containers, sampling, testing, transportation and disposal of all waste.  No work shall begin until the Contractor furnishes the Engineer with a written waste disposal plan.  Any alternative method for handling waste shall be pre-approved by the Engineer.

Southern Logistics, Inc. – 312 Orville Wright Dr., Greensboro, NC 27409

(Ph. 336-662-0292)

A&D Environmental – PO Box 484, High Point, NC 27261

(Ph. 336-434-7750)

Poseidon Environmental Services, Inc. – 837 Boardman-Canfield Rd #209, Youngstown, OH

(Ph. 330-726-1560)

Clean Harbors Reidsville, LLC – 208 Watlington Industrial Drive, Reidsville, NC 27320

(Ph. 336-342-6106)

All removed paint and spent abrasive media shall be tested for lead following the SW-846 TCLP Method 1311 Extraction, as required in 40 CFR 261, Appendix 11, to determine whether it shall be disposed of as hazardous waste.  Furnish the Engineer certified test reports showing TCLP results and Iron analysis of the paint chips stored on site, with disposal in accordance with “Flowchart on Lead Waste Identification and Disposal” at:

http://portal.ncdenr.org/c/document_library/get_file?p_l_id=38491&folderId=328599& name=DLFE-9855.pdf.

All sampling shall be done in presence of the Engineer’s representative.

The Competent Person shall obtain composite samples from each barrel of the wash water and waste generated by collecting two or more portions taken at regularly spaced intervals during accumulation.  Composite the portions into one sample for testing purposes.  Acquire samples after 10% or before 90% of the barrel has accumulated.   The intent is to provide samples that are representative of widely separated portions, but not the beginning and end of wash water or waste accumulation.

Perform sampling by passing a receptacle completely through the discharge stream or by completely diverting the discharge into a sample container.  If discharge of the wash water or waste is too rapid to divert the complete discharge stream, discharge into a container or transportation unit sufficiently large to accommodate the flow and then accomplish the sampling in the same manner as described above.

Comply with the NCDENR Hazardous Waste Compliance Manual for Generators of Hazardous Waste.  Record quantities of waste by weight and dates of waste generation.  Until test results are received, store all waste, and label as “NCDOT Bridge Paint Removal Waste - Pending Analysis” and include the date generated and contact information for the Division HazMat Manager or Project Engineer.  Store waste containers in an enclosed, sealed and secured storage container protected from traffic from all directions.  Obtain approval for the protection plan for these containers from the Engineer.  If adequate protection cannot be obtained by use of existing guardrail, provide the necessary supplies and equipment to maintain adequate protection.  Once test results are received and characterized, label waste as either “Hazardous Waste - Pending Disposal” or “Paint Waste - Pending Disposal”.

Once the waste has been collected, and the quantities determined, prepare the appropriate shipping documents and manifests and present them to the Engineer.  The Engineer will verify the type and quantity of waste and obtain a Provisional EPA ID number from the:

NC Hazardous Waste Section

North Carolina Department of Environment & Natural Resources

1646 Mail Service Center

Raleigh, NC 27699

Phone (919) 508-8400,  Fax (919) 715-4061

At the time of shipping, the Engineer will sign, date and add the ID number in the appropriate section on the manifest.  The maximum on-site storage time for collected waste shall be 90 days.  All waste whether hazardous or non-hazardous will require numbered shipping manifests.  The cost for waste disposal (including lab and Provisional EPA ID number) is included in the bid price for this contract.  Note NC Hazardous Waste Management Rules (15A NCAC 13A) for more information.  Provisional EPA ID numbers may be obtained at this link:

http://portal.ncdenr.org/web/wm/provisional-hw-notification-page.

Testing labs shall be certified in accordance with North Carolina State Laboratory Public Health Environmental Sciences.  List of certified laboratories may be obtained at this link:

http://slphreporting.ncpublichealth.com/EnvironmentalSciences/Certification/CertifiedLaboratory.asp.

All test results shall be documented on the lab analysis as follows:

- For leachable lead:

a.  Soils/Solid/Liquid- EPA 1311/200.7/6010

Area sampling will be performed for the first 2 days at each bridge location.  The area sample will be located within five feet of the containment and where the highest probability of leakage will occur (access door, etc.).  Results from the area sampling will be given to the Engineer within 72 hours of sampling (excluding weekends).  If the results of the samples exceed 20 µg/m3 corrective measures shall be taken and monitoring shall be continued until 2 consecutive sample results are less than 20 µg/m3.

TWA may suspend the work if there are visible emissions outside the containment enclosure or pump monitoring results exceeding the level of 30 µg/m3.

Where schools, housing and/or buildings are within 500 feet of the containment, the Contractor shall perform initial TSP-Lead monitoring for the first 10 days of the project during abrasive blasting, vacuuming and containment removal.  Additional monitoring will be required during abrasive blasting 2 days per month thereafter.  Results of the TSP monitoring at any location shall not exceed 1.5 µg/m3.

## Equipment Mobilization

The equipment used in any travel lanes and paved shoulder shall be mobile equipment on wheels that has the ability to move on/off the roadway in less than 30 minutes.  All work conducted in travel lanes shall be from truck or trailer supported platforms and all equipment shall be self-propelled or attached to a tow vehicle at all times.

## Quality Control Inspector

Provide a quality control inspector in accordance with the SSPC QP guidelines to ensure that all processes, preparation, blasting and coating application are in accordance with the requirements of the contract.   The inspector shall have written authority to perform QC duties to include continuous improvement of all QC internal procedures. The presence of the engineer or inspector at the work site shall in no way lessen the contractor's responsibility for conformity with the contract.

## Quality Assurance Inspector

The quality assurance inspector which may be a Department employee or a designated representative of the Department shall observe, document, assess and report that the Contractor is complying with all of the requirements of the contract.  Inspectors employed by the Department are authorized to inspect all work performed and materials furnished.  Such inspection may extend to all or any part of the work and to the preparation, fabrication or manufacture of the materials to be used.  The inspector is not authorized to alter or waive the requirements of the contract.  Each stage in preparing the structure to be coated which includes but not limited to washing, blasting, coating testing and inspection shall be inspected and approved by the Engineer or his authorized representative.

## Subletting of Contract

Only contractors certified to meet SSPC QP 2, Category A, and have successfully completed lead paint removal and field painting on all similar structures within 18 months prior to this bid are qualified for this work.  Work is only sublet by approval of the Engineer.

## Preparation of Surfaces

Before any other surface preparation is conducted, all surfaces shall be power washed to remove dust, salts, dirt and other contaminants.  All wash water shall be contained, collected and tested in accordance with the requirements of NCDOT Managing Bridge Wash Water specification.  Obtain approval of the Engineer and allow all cleaned surfaces to dry to the touch and without standing water before beginning surface preparation or painting activities.

Surface preparation is done with materials meeting Article 1080-13 of the 2012 Standard Specifications.  No silica sand or other silica materials are permitted for use.  The profile shall be between 1.0 and 3.0 mils when measured on a smooth steel surface.  Conduct and document at least 2 tests per beam/girder and 2 tests per span of diaphragms/cross bracing.

Spread tarpaulins over all pavements and surfaces underneath equipment used for abrasive blasting as well as equipment and containers used to collect abrasive media.  This requirement will be enforced during activity and inactivity of equipment.

Before the Contractor departs from the work site at the end of the work day, collect all debris generated during surface preparation and all dust collector hoses, tarps or other appurtenances containing blasting residue in approved containers.

Clean a 3" x 3" area at each structure to demonstrate the specified finish, and the inspector will preserve this area by covering it with tape, plastic or some other suitable means so that it can be retained as the Dry Film Thickness (DFT) gauge adjustment standard.  An acceptable alternative is for the Contractor to provide a steel plate with similar properties and geometry as the substrate to be measured.

The contractor and or quality assurance representative shall notify the Engineer of any area of corroded steel which has lost more than 50% of its original thickness.

All parts of the bridges not to be painted and the travelling public shall be protected from overspray.  Submit a plan to protect all parts of bridge that are not required to be painted and a plan to protect the traveling public and surrounding environment while applying all coats of paint to a structure.

Ensure that chloride levels on the surfaces are 7 µg/cm2 or lower using an acceptable sample method in accordance with SSPC Guide 15.  The frequency of testing shall be 2 tests per span after all surface preparation has been completed and immediately prior to painting.  Select test areas representing the greatest amount of corrosion in the span as determined by the Engineers’ representative.  Additional testing may be required if significant amounts of chloride are detected.

All weld splatter, slag or other surface defects resulting in a raised surface above the final paint layer shall be removed prior to application of primer coat.

## Painting of Steel

Paint System 1, as specified in these special provisions and Section 442 of the 2012 Standard Specifications, is to be used for this work.  System 1 is an inorganic zinc primer, two coats acrylic paint and one stripe coat of acrylic paint over blast cleaned surfaces in accordance with SSPC-SP-10 (Near White Blast).  Perform all mixing operations over an impervious surface with provisions to prevent runoff to grade of any spilled material.  The contractor is responsible for reporting quantities of thinner purchased as well the amounts used.  No container with thinner shall be left uncovered, when not in use.

Apply 2" stripe coat, by brush or roller only, to all exposed edges of steel including fasteners before applying the finish coat.  Locate the edge or corner in the approximate center of the paint stripe.

Any area where newly applied paint fails to meet the specifications shall be repaired or replaced by the Contractor.  The Engineer approves all repair processes before the repair is made.  Repaired areas shall meet the specifications.  The Contractor applies an additional finish coat of paint to areas where the tape adhesion test is conducted.

## Materials

Only paint suppliers that have a NCDOT qualified inorganic zinc primer may furnish paints for this project.  All paints applied to a structure shall be from the same supplier.  Before any paints are applied the Contractor shall provide the Engineer a manufacturer’s certification that each batch of paint meets the requirements of the applicable Section 1080 of the 2012 Standard Specifications.

The inspector randomly collects a one pint sample of each paint product used on the project.  Additional samples may be collected as needed to verify compliance to the specifications.

Do not expose paint materials to rain, excessive condensation, long periods of direct sunlight, or temperatures above 110°F or below 40°F.  In addition, the Contractor shall place a device which records the high, low and current temperatures inside the storage location.  Follow the manufacturer’s storage requirements if more restrictive than the above requirements.

## Inspection

Surface Preparation for System 1 shall be in accordance with SSPC SP-10.  Any area(s) not meeting the requirements of SSPC SP-10 shall be remediated prior to application of coating.  Surface inspection is considered ready for inspection when all blast abrasive, residue and dust is removed from surfaces to be coated.

(A)	Quality Assurance Inspection

The Contractor furnishes all necessary OSHA approved apparatus such as ladders, scaffolds and platforms as required for the inspector to have reasonable and safe access to all parts of the work.  The contractor illuminates the surfaces to be inspected to a minimum of 50-foot candles of light. All access points shall be illuminated to a minimum of 20-foot candles of light.

NCDOT reserves the right for ongoing QA (Quality Assurance) inspection to include but not limited to surface contamination testing, adhesion pull testing and DFT readings as necessary to assure quality.

Inform the Engineer and the Division Safety Engineer of all scheduled and unannounced inspections from SSPC, OSHA, EPA and/or others that come on site.  Furnish the Engineer a copy of all inspection reports except for reports performed by a third party and or consultant on behalf of the Contractor.

(B)	Inspection Instruments

At a minimum, furnish the following calibrated instruments and conduct the following quality control tests:

(1)	Sling Psychrometer - ASTM E337 - bulb type

(2)	Surface Temperature Thermometer

(3)	Wind Speed Indicator

(4)	Tape Profile Tester - ASTM D4417 Method C

(5)	Surface Condition Standards - SSPC VIS-1 and VIS-3

(6)	Wet Film Thickness Gage - ASTM D4414

(7)	Dry Film Thickness Gage - SSPC-PA2 Modified

(8)	Solvent Rub Test Kit - ASTM D4752

(9)	Adhesion Test Kit - ASTM D3359 Method A (Tape Test)

(10)	Adhesion Pull test - ASTM D4541

(11)	Surface Contamination Analysis Kit or (Chloride Level Test Kit)

SSPC Technology Guide 15

(C)	Quality Control

Maintain a daily quality control record in accordance with Article 442-13 of the 2012 Standard Specifications and make such records available at the job site for review by the inspector and submit to the Engineer as directed.  In addition to the information required on M&T-610, submit all Dry Film Thickness (DFT) readings on a form equivalent to M&T-611.

(1)	Measure DFT at each spot on the attached diagram and at the required number of locations as specified below:

(a)	For span members less than 45 feet; three random locations along each girder in each span.

(b)	For span members greater than 45 feet; add one additional location for each additional 10 feet in span length.

DFT measurements for the prime coat shall not be taken for record until the zinc primer has cured in accordance with ASTM D4752 (MEK Rub Test) with no less than a four resistance rating.

Stiffeners and other attachments to beams and or plate girders shall be measured at no less than five random spots per span.  Also dry film thickness is measured at no less than six random spots per span on diaphragms/“K” frames.

Each spot is an average of three to five individual gage readings as defined in SSPC PA-2.  No spot average shall be less than 80% of minimum DFT for each layer applied; this does not apply to stripe coat application.  Spot readings that are non-conforming shall be re-accessed by performing additional spot measurements not to exceed one foot intervals on both sides of the low areas until acceptable spot averages are obtained.  These non-conforming areas shall be corrected by the Contractor prior to applying successive coats.

(2)	Two random adhesion tests (1 test=3 dollies) per span are conducted on interior surfaces in accordance with ASTM D4541 (Adhesion Pull Test) after the prime coat has been properly cured in accordance with ASTM D4752 (MEK Rub Test) with no less than a 4 resistance rating, and will be touched up by the Contractor.  The required minimum average adhesion is 400 psi.

(3)	Cure of the intermediate and stripe coats shall be accessed by using the thumb test in accordance with ASTM D1640 (Curing Formation Test) prior to the application of any successive layers of paint.

(4)	One random Cut Tape adhesion test per span is conducted in accordance with ASTM D3359 (X-Cut Tape Test) on interior surface after the finish coat is cured.  Repair areas shall be properly tapered and touched up by the Contractor.

## Safety and Environmental Compliance Plans

Personnel access boundaries are delineated for each work site using signs, tape, cones or other approved means.  Submit copies of safety and environmental compliance plans that comply with SSPC QP 2 Certification requirements.

## Health and Safety Responsibilities

This project may involve toxic metals such as arsenic, lead, cadmium and hexavalent chromium.  It is the contractor’s responsibility to test for toxic metals and if found, comply with the OSHA regulations, which may include medical testing.

Ensure a “Competent Person” as defined in OSHA 29 CFR 1926.62; one who is capable of identifying existing and predictable hazards in the surroundings or working conditions which are unsanitary, hazardous, or dangerous to employees, and who has authorization to take prompt corrective measures to eliminate them; is on site during all surface preparation activities and monitors the effectiveness of containment, dust collection systems and waste sampling.  Before any work begins, provide a written summary of the Competent Person’s safety training.

Comply with Subarticle 442-14(B) of the 2012 Standard Specifications.

Comply with Subarticle 442-14(D) of the 2012 Standard Specifications.  Ensure employee blood sampling test results are less than 50 micrograms per deciliter.  Remove employees with a blood sampling test of 50 or more micrograms per deciliter from work activities involving any lead exposure.

An employee who has been removed with a blood level of 50 micrograms per deciliter or more shall have two consecutive blood sampling tests spaced one week apart indicating that the employee’s blood lead level is at or below 40 micrograms per deciliter before returning to work activities involving any lead exposure.

All OSHA recordable accidents that occur during the project duration are to be reported to the Engineer within twenty-four (24) hours of occurrence.  In addition, for accidents that involve civilians or property damage that occurs within the work zone the Division Safety Engineer shall be notified immediately.

Prior to blasting operations, the Contractor shall have an operational OSHA approved hand wash station at each bridge location and a decontamination trailer at each bridge or between bridges unless the work is on the roadway, or the Contractor shall show reason why it is not feasible to do so and provide an alternative site as approved by the Engineer.  The Contractor shall assure that all employees whose airborne exposure to lead is above the PEL shall shower at the end of their work shift.

## Storage of Paint and Equipment

Provide a location for materials, equipment and waste storage.  Spread tarpaulins over all pavements and surfaces underneath equipment used for abrasive recycling and other waste handling equipment or containers.  All land and or lease agreements that involve private property shall disclose to the property owner that heavy metals may be present on the Contractor’s equipment.  Prior to storing the Contractor’s equipment on private property, provide a notarized written consent signed by the land owner received by the Engineer at least forty-eight (48) hours before using property.   All storage of paint, solvents and other materials applied to structures shall be stored in accordance with Section 442 of the 2012 Standard Specifications or the manufacturers’ requirements.  The more restrictive requirements will apply.

## Utilities

Protect all utility lines or mains which may be supported on, under, or adjacent to bridge work sites from damage and paint overspray.

## Measurement and Payment

The cost of inspection, surface preparation and repainting the existing structure is included in the lump sum price bid for Painting Existing Structure.  This price is full compensation for furnishing all inspection equipment, all paint, cleaning abrasives, cleaning solvents and all other materials; preparing and cleaning surfaces to be painted; applying paint in the field; protecting work area, traffic and property; and furnishing blast cleaning equipment, paint spraying equipment, brushes, rollers, any other hand or power tools and any other equipment; and a containment enclosure.

Pollution Control will be paid at the contract lump sum price which will be full compensation for all collection, handling, storage, air monitoring, and disposal of debris and wash water, all personal protective equipment, and all personal hygiene requirements, and all equipment, material and labor necessary for the daily collection of the blast debris into specified containers; and any measures necessary to ensure conformance to all safety and environmental regulations as directed by the Engineer.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Painting Existing Structure | Lump Sum |
| Pollution Control | Lump Sum |

# Text boxes

Less than 36" in height and/or bottom flanges less than 16" in width.

7 Spot Areas

21 Individual DFT Readings

7 Spot Areas

21 Individual DFT Readings

E1

C1

C2

A1

*D

A2

*D

B1

B2

*D areas are only included when flange thickness is one inch (1") or greater.

36" in height or greater and/or bottom flanges greater than 16" in width.

10 Spot Areas

30 Individual DFT Readings

7 Spot Areas

21 Individual DFT Readings

D1

C1

C2

A1

*D

A2

*D2

B1, B2

F1, F2

*D areas are only included when flange thickness is one inch (1") or greater.

D2