# EPOXY OVERLAY SYSTEM II	(08-08-22)

## General

This special provision is intended for use on bridges with an Average Daily Traffic (ADT) less than or equal to 5,000.  This work shall consist of furnishing and applying an epoxy overlay system over the concrete bridge deck in accordance with the contract documents and consists of a minimum of two (2) layers of hybrid polymer resins with a special blend of extremely hard aggregate designed to provide a ⅜”thick overlay for the purpose of crack treatment, complete waterproofing, and providing a non-skid surface.  The overlay system shall be formulated and applied to withstand continuous heavy traffic, extreme changes in weather conditions, and deformations due to structure loading and temperature changes.

## Performance Guarantee

The Contractor shall provide a 36-month performance guarantee bond to the Department, in addition to the 12-month guarantee, for the wearing surface materials and workmanship against latent and patent defects arising from faulty materials, poor workmanship or negligence for a period of 36 months against defects such as, but not limited to, delamination of the epoxy overlay from the deck surface, delamination of aggregate, peeling and blistering.

The guarantee period will start on the date of project final acceptance. This applies to the 36-month performance guarantee bond, as well as the 12-month guarantee.

The performance guarantee bond will be invoked if 25 square feet or more of the deck surface with defects prior to the end of the 36-month project guarantee period.  The Contractor shall replace defective materials and workmanship at no cost to the Department. The Contractor will not be responsible for damage due to normal wear and tear, or use in excess of the design.

The performance guarantee bond amount shall be the bid quantity of epoxy overlay multiplied by the statewide average unit bid price for the epoxy overlay. The guarantee period of 36 months and bond value shall be specified in the performance guarantee bond provided to the Department prior to final acceptance of the project.  To ensure uniform administration statewide, the Division Engineer will forward details regarding the circumstances surrounding any proposed guarantee repairs to the Chief Engineer for review and approval prior to the repairs being performed.

## Materials

This two-part epoxy polymer overlay system shall be on the NCDOT Approved Products List (APL) and be free of any fillers or volatile solvents and shall be formulated to provide a simple volumetric mixing ratio of two components such as one to one (1:1) or two to one (2:1) by volume.  The epoxy overlay system shall be formulated to provide flexibility in the system without any sacrifice of the hardness, chemical resistance or strength of the system.  Use of external/conventional flexibilizers will not be accepted.  Flexibility shall be by interaction of elastomers which chemically link during the process of curing so the flexibility of the molecule is least affected during the low temperature conditions that are confronted in actual use.

The Contractor shall submit a Certified Test Report from independent labs for all of the materials associated with the overlay in accordance with this special provision.

All components shall be shipped in strong, substantial containers, bearing the manufacturer’s label specifying batch/lot number, brand name, and quantity.  If bulk resin is to be used, the contractor shall notify the Engineer in writing ten (10) working days prior to the delivery of the bulk resin to the job site.  Bulk resin is any resin that is stored in containers in excess of 55 gallons.

- Epoxy

When the two component system is mixed at the appropriate ratio, the cured resin shall conform to the following requirements:

| EPOXY PROPERTIES |  |  |
| --- | --- | --- |
| Property | Requirement | Test Method |
| Viscosity-Poises at 77°F ± 2°F | 7-25 | AASHTO 7237 |
| Pot Life | 15-45 minutes @ 75° F | ASTM C881 |
| Min. Tensile Strength at 7 days | 2000 psi | ASTM D638 |
| Tensile Elongation at 7 days | 30-70% | ASTM D638 |
| Min. Compressive Strength @ 3 hrs. | 1,000 psi | ASTM C109 |
| Min. Compressive Strength @ 24 hrs. | 5000 psi | ASTM C109 |
| Min. adhesion strength @ 24 hrs. | 250 psi @ 75° F | ASTM C1583 |
| Max. Water Absorption | 1% | ASTM D570 |

- Aggregate

Aggregate used for all layers shall be non-friable, non-polishing, clean and free from surface moisture.  Unless otherwise approved by the Engineer, the aggregate shall be flint rock, basalt, or calcined bauxite, 100% fractured, thoroughly washed and kiln dried to a maximum moisture content of 0.2% by weight, measured in accordance with ASTM C566.  The fracture requirements shall be at least one mechanically fractured face and will apply to materials retained on a U.S. No. 10 sieve.  Calcined bauxite shall have a minimum aluminum oxide content of 87%, in accordance with ASTM C25. Aggregate shall conform to the following requirements:

| AGGREGATE PROPERTIES |  |  |  |  |
| --- | --- | --- | --- | --- |
| Property |  | Value |  | Test Method |
| Moisture Content, max. |  | 0.2% by weight |  | AASHTO T255 |
| Mohs Hardness, min. |  | 7 |  |  |
| Soundness Loss, 5 cycles in Sodium Sulfate, max. |  | 5.4% |  | AASHTO T104 |
| Micro-Deval, max. |  | 10% |  | AASHTO T327 |
| AGGREGATE GRADATION |  |  |
| Sieve | Percent Passing |  |
| No. 4 | 100 |  |
| No. 8 | 30-75 |  |
| No. 16 | Max. 5 |  |
| No. 30 | Max. 1 |  |

| AGGREGATE ABSORPTION PROPERTIES |  |  |
| --- | --- | --- |
| Aggregate Type | Value | Test Method |
| Flint | < 3.5% | ASTM C128 |
| Basalt | < 2% | ASTM C128 |
| Calcined Bauxite | < 1.5% | ASTM C128 |

## Surface Preparation

Remove all existing overlays if applicable, and all loose, disintegrated, unsound or contaminated concrete from the bridge deck.  Prepare the bridge deck prior to applying the overlay system, in accordance with the manufacturer's recommendations, the special provision Concrete Deck Repair for Epoxy Overlay, and this special provision.

Prior to overlay placement and upon completion of the deck repairs, clean the entire deck surface by steel shot blasting and other means to remove asphaltic material, oils, dirt, rubber, curing compounds, pavement markings, paint carbonation, laitance, weak surface mortar and other materials that may interfere with the bonding or curing of the overlay.  Do not begin shot-blasting until all grinding or milling operations are completed.  Use sandblasting equipment on areas that cannot be reached by the shot-blasting operation.  If expansion joints are not being replaced or have been replaced prior to shot-blasting they shall be protected from damage from the shot-blasting operation.  Pavement markings shall be considered clean when the concrete has exposed aggregate showing through the paint stripe.  Deck drains and areas of curb or railing above the proposed surface shall be protected from the shot-blasting operation.  Mortar that is soundly bonded to the coarse aggregate shall have open pores to be considered adequate for bond.  Provide a self-propelled vacuum capable of picking up dust and other loose material from the shot-blasting operation.  Provide air compressors equipped with oil/water separators, capable of blowing off all remaining dust and debris, and drying all moisture from the bridge deck.  Care shall be taken and methods used to fully capture and collect the excess material.

Prior to overlay placement and upon completion of surface preparation, perform bond testing of the epoxy overlay material in accordance with ASTM C1583 on two (2) pre-selected 1.5’ x 3’ test patches.  Test locations will be determined by the Engineer.  The average minimum bond strength of the epoxy overlay system on normal weight concrete shall be 250 psi, with no individual test measured below 225 psi.  An acceptable test will demonstrate that the overlay bond strength is sufficient, or by producing a concrete subsurface failure area greater than 50% of the test surface area.Install test sections with the same materials, equipment, personnel, timing and sequence of operations and curing time that will be used for the installation of the overlay.  Test locations shall be repaired with approved repair materials.

If the cleaning method, materials and installation procedure do not produce acceptable test results, the contractor must remove failed test patches, make the necessary adjustments, and retest all patches at no additional cost to the Department until satisfactory test results are obtained.

Epoxy based overlays shall not be placed on hydraulic cement concrete that is less than 28 days old.  Patching and cleaning operations shall be inspected and approved prior to placing each layer of the overlay.  Any contamination of the deck or intermediate courses, after initial cleaning, shall be removed.

The deck shall be completely dry at the time of application of the epoxy concrete overlay.  Deck drains shall be closed off during application of epoxy overlay.

## Equipment

For mechanical applications, equipment shall consist of no less than an epoxy distribution system, aggregate spreader, application squeegee, vacuum truck, and a source of lighting if work is to be performed at night.  The distribution system shall accurately measure and mix the epoxy resin and hardening agent, and shall uniformly and accurately apply the epoxy materials at the specified rate to the bridge deck in such a manner as to cover 100% of the work area.  The aggregate spreader shall be propelled in such a manner as to uniformly and accurately apply the aggregate to cover 100% of the epoxy material.  Aggregate shall be sprinkled or dropped vertically in a manner such that the level of the epoxy mixture is not disturbed.   The vacuum truck shall be self-propelled.

For hand applications, equipment shall consist of calibrated containers, a “jiffy” type paddle mixer or other paddle designed specifically for epoxy mixing, squeegees, rollers and brooms, which are suitable for mixing the epoxy and applying the epoxy and aggregate.  Paddle shall remain submerged when mixing to avoid entraining air. Equipment shall uniformly and accurately apply the epoxy materials at the specified rate to the bridge deck, in such a manner as to cover 100% of the work area. The aggregate shall be applied in such a manner as to uniformly and accurately cover 100% of the epoxy material. Aggregate shall be sprinkled or dropped vertically in a manner such that the level of the epoxy mixture is not disturbed.

## Application

Handling and mixing of the epoxy resin and hardening agent shall be performed in a safe manner to achieve the desired result in accordance with the manufacturer's recommendations as approved and as directed by the Engineer.  Epoxy overlay materials shall not be placed when weather or surface conditions are such that the material cannot be properly handled, placed, spread and cured within the specified requirements of traffic control.

The application rates of the liquid and stone in the two (2) layers shall be as recommended by the manufacturer, but not less than the following rate of application.

| TABLE 4 |  |  |
| --- | --- | --- |
| APPLICATION RATES |  |  |
| Course | Min. Epoxy Rate (Gal./100 SF) | Min. Aggregate Rate (Lbs./Sq.Yd) |
| 1 | 2.5 | 10 |
| 2 | 5 | 14 |

The final overlay thickness shall be a minimum of ⅜”.  Once the epoxy mixture has been prepared, immediately and uniformly applied it to the surface of the bridge deck.  There shall be no longitudinal joints of the epoxy overlay in the wheel path.  The temperature of the bridge deck surface and all epoxy and aggregate components shall be 60°F or above at the time of application.  Epoxy shall not be applied if the air temperature is expected to drop below 55°F within eight (8) hours after application or if air temperatures would cause the gel time to be less than ten (10) minutes.  Consult with the manufacturer when placing overlay at temperatures above 90°F.  The dry aggregate shall be applied in such a manner as to completely cover the epoxy mixture so that no wet spots appear and before it begins to gel.  First course applications that do not receive enough aggregate prior to gel shall be removed and replaced.  A second course insufficiently covered with aggregate may be left in place, but will require additional applications before opening to traffic.  After each course is fully cured, all loose aggregate shall be removed by vacuuming or brooming.  Traffic shall not be allowed on the first course of the overlay.  Traffic and equipment shall not be permitted on the overlay surface during the curing period.    The minimum curing periods shall be as follows:

Course:  Average temperature of deck, epoxy and aggregate components in °F

60-64	65-69	70-74	75-79	80-84	85+

Course 1	4 hrs.	3 hrs.	2.5 hrs.	2 hrs.	1.5 hrs.	1 hr.

Course 2	6.5 hrs.*	5 hrs.	4 hrs.	3 hrs.	3 hrs.	3 hrs.

*Course 2 shall be cured for 8 hrs. if the air temperature drops below 60°F during the curing period.

The Contractor shall plan and execute the work to provide the curing periods as specified herein, or manufacturer proposed curing periods may be submitted to the Engineer for review and approval.

Do not apply epoxy overlay courses over modular joints, metal expansion joints, or foam joint seals.  A bond breaker shall be placed on all expansion joints.

In the event the Contractor's operation damages the epoxy overlay, the Contractor shall remove the damaged areas by saw-cutting in rectangular sections to the top of the concrete deck surface and replacing the various courses in accordance with this special provision at no additional cost to the Department.

Prior to acceptance, perform bond testing for each span or 300 square yards, whichever is smaller, in accordance with ASTM C1583 on 1.5’ x 3’ test patches.  Test locations will be determined by the Engineer.  The average minimum bond strength of the epoxy overlay system on normal weight concrete shall be 250 psi, with no individual test measured below 225 psi.  An acceptable test will demonstrate that the overlay bond strength is sufficient, or by producing a concrete subsurface failure area greater than 50% of the test surface area, Unacceptable test results will require removal and replacement of overlay as directed by the Engineer at no cost to the Department.  Test locations shall be repaired with approved repair materials.

## Measurement & Payment

Epoxy Overlay System II will be measured and paid for at the contract unit price per square feet.  The price shall include surface preparation, furnishing and placing the overlay system, providing a 36-month warranty bond, and all tools, labor, materials, bond strength testing and any incidentals necessary to complete the work.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Epoxy Overlay System II | Square Feet |