COIR FIBER WATTLE BARRIER:

| (5-20-13) | 1630 |  |
| --- | --- | --- |

Description

Coir fiber wattle barriers are tubular products consisting of coir fibers (coconut fibers) encased in coir fiber or synthetic netting and used at the toe of fills or on slopes to intercept runoff.  Coir fiber wattle barriers are to be placed at locations shown on the plans or as directed.  Installation shall follow the detail provided in the plans and as directed.  Work includes furnishing materials, installation, maintenance and removing coir fiber wattle barriers.

Materials

Coir fiber wattle shall meet the following specifications:

| Inner Material | 100% Coir (Coconut) Fibers |
| --- | --- |
| Minimum Diameter | 18" |
| Minimum Length | 10 ft. |
| Minimum Density | 5 lb./c.f. ± 10% |
| Net Material | Coir (Coconut) or Synthetic |
| Net Openings | 2" x 2" |
| Net Strength | 90 lb. |
| Minimum Weight | 10 lb./ft. ± 10% |

Stakes shall be used as anchors.  Provide hardwood stakes a minimum of 2-ft long with a 2" x 2" nominal square cross section.  One end of the stake shall be sharpened or beveled to facilitate driving down into the underlying soil.

Provide staples made of 0.125" diameter new steel wire formed into a U-shape not less than 12" in length with a throat of 1" in width.

Construction Methods

Align coir fiber wattle barriers in an overlapping and alternating pattern.  Excavate a trench the entire length of each wattle with a depth of 2" to 3" for the wattle to be placed.  Secure coir fiber wattle barriers to the soil by wire staples approximately every linear foot and at the end of each wattle.  Install at least 4 stakes on the downslope side of the wattle with a maximum spacing of 2 linear feet and according to the detail.  Install at least 2 stakes on the upslope side of the coir fiber wattle barriers according to the detail provided in the plans.  Drive stakes into the ground at least 10" with no more than 2" projecting from the top of the wattle.  Drive stakes at an angle according to the detail provided in the plans.

For coir fiber wattle barriers used to reduce runoff velocity for large slopes, use a maximum spacing of 25 ft. for the barrier measured along the slope.

Maintain the coir fiber wattle barriers until the project is accepted or until the coir fiber wattle barriers are removed, and remove and dispose of silt accumulations at the coir fiber wattle barriers when so directed in accordance with Section 1630 of the Standard Specifications.

Measurement and Payment

Coir Fiber Wattle Barrier will be measured and paid as the actual number of linear feet of coir fiber wattle barrier installed and accepted.  Such price and payment will be full compensation for all work covered by this provision, including, but not limited to, furnishing all materials, labor, equipment and incidentals necessary to install the coir fiber wattle barrier.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Coir Fiber Wattle Barrier | Linear Foot |